Fantastic report on

input.doc

Distribution:

| Name | Function | 0.1 | 0.5 | 1.0 |
| --- | --- | --- | --- | --- |
| N.N.-999 | Masterking Group Manager (MGM) |  |  |  |
| N.N.-998 | Product Ontwikkelt Manager (POM) |  |  |  |
| N.N.-1 | (AS) |  |  |  |
| N.N.-2 | (DS) |  |  |  |
| N.N.-3 | (BS) |  |  |  |
| T.P. | Supervisor All Coding |  |  |  |

# Table of Contents:

Table of Contents:	2

Anchor Scan Parameters: (Bookmark1)	3

Graphics: (Bookmark2)	4

Peak List: (Bookmark 3)	5

Identified Patterns List: (Bookmark4)	7

Plot of Identified Phases: (Bookmark 5)	7

Document History: (Bookmark 6)	8

# Anchor Scan Parameters: (Bookmark1)

Dataset Name	Ti3C2_2_20190722_1

File name	Y:\James Bird\Training\Ti3C2_2_20190722_1.xrdml

Sample Identification	2

Comment	Run by J E Warren sample queue batch

Configuration=Spinner, Owner=User-1, Creation date=08/12/2015 14:27:11

Goniometer=PW3050/60 (Theta/Theta); Minimum step size 2Theta:0.001; Minimum step size Omega:0.001

Sample stage=Spinner PW3064

Diffractometer system=XPERT-PRO

Measurement program=James Bird 10mm Mask, Owner=User-1, Creation date=22/07/2019 14:48:21

1h 5-70

Measurement Start Date/Time	22/07/2019 16:49:44

Operator	xrduser

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	5.0097

End Position [°2θ]	69.9537

Step Size [°2θ]	0.0330

Scan Step Time [s]	219.7100

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	2.12

Offset [°2θ]	0.0000

Divergence Slit Type	Automatic

Irradiated Length [mm]	8.00

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-Alpha1 [Å]	1.54060

K-Alpha2 [Å]	1.54443

K-Beta [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	40 mA, 40 kV

Diffractometer Type	0000000000007141

Diffractometer Number	0

Goniometer Radius [mm]	240.00

Dist. Focus-Diverg. Slit [mm]	100.00

Incident Beam Monochromator	No

Spinning	Yes

# Graphics: (Bookmark2)

# Peak List: (Bookmark 3)

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] | Tip Width | Matched by |
| --- | --- | --- | --- | --- | --- | --- |
| 5.4129 | 2096.90 | 0.1000 | 16.31346 | 3.91 | 0.1200 |  |
| 5.4263 | 1048.45 | 0.1000 | 16.31346 | 1.96 | 0.1200 |  |
| 5.6920 | 3741.44 | 0.1000 | 15.51400 | 6.98 | 0.1200 |  |
| 5.7062 | 1870.72 | 0.1000 | 15.51400 | 3.49 | 0.1200 |  |
| 5.9082 | 4755.39 | 0.1000 | 14.94679 | 8.88 | 0.1200 |  |
| 5.9229 | 2377.70 | 0.1000 | 14.94679 | 4.44 | 0.1200 |  |
| 6.1068 | 6587.40 | 0.1000 | 14.46129 | 12.29 | 0.1200 |  |
| 6.1219 | 3293.70 | 0.1000 | 14.46129 | 6.15 | 0.1200 |  |
| 6.3176 | 8503.25 | 0.1000 | 13.97918 | 15.87 | 0.1200 |  |
| 6.3333 | 4251.63 | 0.1000 | 13.97918 | 7.94 | 0.1200 |  |
| 6.6016 | 6524.46 | 0.1000 | 13.37841 | 12.18 | 0.1200 |  |
| 6.6180 | 3262.23 | 0.1000 | 13.37841 | 6.09 | 0.1200 |  |
| 9.3514 | 20942.37 | 0.1000 | 9.44966 | 39.09 | 0.1200 | 04-012-0632 |
| 9.3747 | 10471.18 | 0.1000 | 9.44966 | 19.54 | 0.1200 |  |
| 18.9460 | 6157.08 | 0.1000 | 4.68031 | 11.49 | 0.1200 | 04-012-0632 |
| 18.9935 | 3078.54 | 0.1000 | 4.68031 | 5.75 | 0.1200 |  |
| 25.4166 | 299.28 | 0.1000 | 3.50156 | 0.56 | 0.1200 | 04-004-2852 |
| 25.4808 | 149.64 | 0.1000 | 3.50156 | 0.28 | 0.1200 |  |
| 26.7385 | 1141.41 | 0.1000 | 3.33137 | 2.13 | 0.1200 |  |
| 26.8062 | 570.70 | 0.1000 | 3.33137 | 1.07 | 0.1200 |  |
| 27.0397 | 1196.59 | 0.1000 | 3.29495 | 2.23 | 0.1200 | 04-003-0648 |
| 27.1081 | 598.30 | 0.1000 | 3.29495 | 1.12 | 0.1200 |  |
| 27.4946 | 566.21 | 0.1000 | 3.24145 | 1.06 | 0.1200 |  |
| 27.5643 | 283.11 | 0.1000 | 3.24145 | 0.53 | 0.1200 |  |
| 28.6934 | 505.65 | 0.1000 | 3.10869 | 0.94 | 0.1200 | 04-012-0632 |
| 28.7662 | 252.82 | 0.1000 | 3.10869 | 0.47 | 0.1200 |  |
| 33.8547 | 2571.25 | 0.1000 | 2.64563 | 4.80 | 0.1200 | 04-012-0632 |
| 33.9414 | 1285.63 | 0.1000 | 2.64563 | 2.40 | 0.1200 |  |
| 34.9889 | 874.25 | 0.1000 | 2.56243 | 1.63 | 0.1200 | 04-004-2852 |
| 35.0786 | 437.12 | 0.1000 | 2.56243 | 0.82 | 0.1200 |  |
| 35.7690 | 3163.33 | 0.1000 | 2.50830 | 5.90 | 0.1200 | 04-004-2919, 04-003-0648 |
| 35.8609 | 1581.67 | 0.1000 | 2.50830 | 2.95 | 0.1200 |  |
| 36.5836 | 1110.18 | 0.1000 | 2.45430 | 2.07 | 0.1200 | 04-012-0632 |
| 36.6777 | 555.09 | 0.1000 | 2.45430 | 1.04 | 0.1200 |  |
| 38.6357 | 53578.35 | 0.1000 | 2.32853 | 100.00 | 0.1200 | 04-012-0632 |
| 38.7356 | 26789.18 | 0.1000 | 2.32853 | 50.00 | 0.1200 |  |
| 41.5609 | 13611.52 | 0.1000 | 2.17115 | 25.40 | 0.1200 | 04-004-2852, 04-004-2919, 04-012-0632 |
| 41.6690 | 6805.76 | 0.1000 | 2.17115 | 12.70 | 0.1200 |  |
| 43.2031 | 705.45 | 0.1000 | 2.09235 | 1.32 | 0.1200 | 04-004-2852 |
| 43.3159 | 352.73 | 0.1000 | 2.09235 | 0.66 | 0.1200 |  |
| 44.7577 | 291.17 | 0.1000 | 2.02322 | 0.54 | 0.1200 | 04-012-0632 |
| 44.8750 | 145.59 | 0.1000 | 2.02322 | 0.27 | 0.1200 |  |
| 48.2884 | 1175.89 | 0.1000 | 1.88321 | 2.19 | 0.1200 | 04-012-0632 |
| 48.4161 | 587.95 | 0.1000 | 1.88321 | 1.10 | 0.1200 |  |
| 52.1101 | 398.79 | 0.1000 | 1.75373 | 0.74 | 0.1200 | 04-012-0632 |
| 52.2493 | 199.39 | 0.1000 | 1.75373 | 0.37 | 0.1200 |  |
| 52.3875 | 314.05 | 0.1000 | 1.74510 | 0.59 | 0.1200 | 04-004-2852 |
| 52.5276 | 157.03 | 0.1000 | 1.74510 | 0.29 | 0.1200 |  |
| 53.5935 | 385.92 | 0.1000 | 1.70864 | 0.72 | 0.1200 |  |
| 53.7373 | 192.96 | 0.1000 | 1.70864 | 0.36 | 0.1200 |  |
| 53.9605 | 456.93 | 0.1000 | 1.69788 | 0.85 | 0.1200 | 04-003-0648 |
| 54.1055 | 228.47 | 0.1000 | 1.69788 | 0.43 | 0.1200 |  |
| 56.2737 | 2048.09 | 0.1000 | 1.63345 | 3.82 | 0.1200 | 04-012-0632, 04-003-0648 |
| 56.4260 | 1024.04 | 0.1000 | 1.63345 | 1.91 | 0.1200 |  |
| 57.3586 | 994.17 | 0.1000 | 1.60510 | 1.86 | 0.1200 | 04-004-2852 |
| 57.5144 | 497.09 | 0.1000 | 1.60510 | 0.93 | 0.1200 |  |
| 60.0578 | 2487.76 | 0.1000 | 1.53925 | 4.64 | 0.1200 | 04-012-0632 |
| 60.2225 | 1243.88 | 0.1000 | 1.53925 | 2.32 | 0.1200 |  |
| 60.3173 | 1772.80 | 0.1000 | 1.53325 | 3.31 | 0.1200 | 04-004-2919 |
| 60.4828 | 886.40 | 0.1000 | 1.53325 | 1.65 | 0.1200 |  |
| 60.7021 | 867.77 | 0.1000 | 1.52445 | 1.62 | 0.1200 | 04-012-0632 |
| 60.8689 | 433.89 | 0.1000 | 1.52445 | 0.81 | 0.1200 |  |
| 65.3302 | 879.67 | 0.1000 | 1.42720 | 1.64 | 0.1200 | 04-012-0632 |
| 65.5129 | 439.83 | 0.1000 | 1.42720 | 0.82 | 0.1200 |  |
| 68.0706 | 407.21 | 0.1000 | 1.37626 | 0.76 | 0.1200 | 04-004-2852 |
| 68.2631 | 203.61 | 0.1000 | 1.37626 | 0.38 | 0.1200 |  |

# Identified Patterns List: (Bookmark4)

| Visible | Ref.Code | Score | Compound Name | Displ.[°2θ] | Scale Fac. | Chem. Formula |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-004-2852 | 37 | Aluminum Oxide | -0.183 | 0.009 | Al2 O3 |
| * | 04-004-2919 | 30 | Titanium Carbide | -0.190 | 0.073 | Ti C |
| * | 04-012-0632 | 25 | Titanium Aluminum Carbide | -0.214 | 0.276 | Ti3 Al C2 |
| * | 04-003-0648 | 19 | Titanium Oxide | -0.358 | 0.030 | Ti O2 |

# Plot of Identified Phases: (Bookmark 5)

# Document History: (Bookmark 6)

Beam attenuation factor(s) used to back-calculate ESDs:

- Modification time = "19/09/2019 09:34:28"

- Modification editor = "xrdpc2"

Insert Measurement:

- File name = "Ti3C2_2_20190722_1.xrdml"

- Modification time = "19/09/2019 09:34:28"

- Modification editor = "xrdpc2"

Default properties:

- Measurement step axis = "None"

- Internal wavelengths used from anode material: Copper (Cu)

- Original K-Alpha1 wavelength = "1.54060"

- Used K-Alpha1 wavelength = "1.54060"

- Original K-Alpha2 wavelength = "1.54443"

- Used K-Alpha2 wavelength = "1.54443"

- Original K-Beta wavelength = "1.39225"

- Used K-Beta wavelength = "1.39225"

- Fixed div. slit size = "1.00000"

- Receiving slit size = "0.10000"

- Step axis value = "0.00000"

- Offset = "0.00000"

- Sample length = "10.00000"

- Modification time = "19/09/2019 09:34:28"

- Modification editor = "xrdpc2"

Interpolate Step Size:

- Initial Scan Range = 5.00971 - 69.98310

- Initial Step Size = 0.03342

- Derived Step Size = 0.03300

- Use Derived Step Size = "Yes"

- Modification time = "19/09/2019 09:34:28"

- Modification editor = "PANalytical"

Take As Anchor Scan:

- Scan name = "Ti3C2_2_20190722_1"

- Modification time = "19/09/2019 09:41:32"

- Modification editor = "xrdpc2"

Take As Anchor Scan:

- Scan name = "Ti3C2_2_20190722_1"

- Modification time = "19/09/2019 09:50:29"

- Modification editor = "xrdpc2"

Take As Anchor Scan:

- Scan name = "Ti3C2_2_20190722_1"

- Modification time = "19/09/2019 09:58:16"

- Modification editor = "xrdpc2"

Determine Background:

- Add to net scan = "Nothing"

- User defined intensity = "-5"

- Correction method = "Automatic"

- Bending factor = "5"

- Minimum significance = "0.7"

- Minimum tip width = "0"

- Maximum tip width = "1"

- Peak base width = "2"

- Use smoothed input data = "Yes"

- Granularity = "20"

- Modification time = "22/02/2001 10:17:43"

- Modification editor = "PANalytical"

Take As Anchor Scan:

- Scan name = "Ti3C2_2_20190722_1"

- Modification time = "19/09/2019 11:33:49"

- Modification editor = "xrdpc2"

Search Peaks:

- Minimum significance = "1"

- Minimum tip width = "0.01"

- Maximum tip width = "1"

- Peak base width = "2"

- Method = "Minimum 2nd derivative"

- Modification time = "19/09/2019 11:33:59"

- Modification editor = "PANalytical"

Profile/Rietveld fitting:

- Angular range Gonio = "5.010 - 12.567"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "8"

- Chi Square = "21.6271763813582"

- Rp = "0.22987"

- Rwp = "0.30972"

- Rexp = "0.01432"

- Modification time = "19/09/2019 11:34:27"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "5.4080"

- Modification time = "19/09/2019 11:34:33"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "5.6604"

- Modification time = "19/09/2019 11:34:34"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "5.9248"

- Modification time = "19/09/2019 11:34:34"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "6.1532"

- Modification time = "19/09/2019 11:34:35"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "6.6100"

- Modification time = "19/09/2019 11:34:36"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "5.010 - 12.567"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "28"

- Chi Square = "9.32312595151828"

- Rp = "0.09575"

- Rwp = "0.12736"

- Rexp = "0.01366"

- Modification time = "19/09/2019 11:34:42"

- Modification editor = "xrdpc2"

Delete Peak(s):

- Start position = "12.7687"

- End position = "12.7687"

- Modification time = "19/09/2019 11:34:57"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "15.768 - 23.325"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "4"

- Chi Square = "1.18270669199686"

- Rp = "0.01931"

- Rwp = "0.02494"

- Rexp = "0.02109"

- Modification time = "19/09/2019 11:35:05"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "23.028 - 30.585"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "16"

- Chi Square = "4.05623967416973"

- Rp = "0.05097"

- Rwp = "0.07927"

- Rexp = "0.01954"

- Modification time = "19/09/2019 11:35:16"

- Modification editor = "xrdpc2"

Delete Peak(s):

- Start position = "25.1172"

- End position = "25.1807"

- Modification time = "19/09/2019 11:35:27"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "23.028 - 30.585"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "12"

- Chi Square = "3.99112561883573"

- Rp = "0.05087"

- Rwp = "0.07872"

- Rexp = "0.01972"

- Modification time = "19/09/2019 11:35:32"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "26.7676"

- Modification time = "19/09/2019 11:35:37"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "23.028 - 30.585"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "16"

- Chi Square = "3.04165015741079"

- Rp = "0.04059"

- Rwp = "0.05944"

- Rexp = "0.01954"

- Modification time = "19/09/2019 11:35:43"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "27.5729"

- Modification time = "19/09/2019 11:35:45"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "23.028 - 30.585"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "20"

- Chi Square = "2.56102342513463"

- Rp = "0.03454"

- Rwp = "0.04958"

- Rexp = "0.01936"

- Modification time = "19/09/2019 11:35:51"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "32.307 - 37.224"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "16"

- Chi Square = "1.28522254625086"

- Rp = "0.01930"

- Rwp = "0.02457"

- Rexp = "0.01912"

- Modification time = "19/09/2019 11:36:12"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "37.257 - 39.567"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "8"

- Chi Square = "12.6986561287879"

- Rp = "0.10357"

- Rwp = "0.13417"

- Rexp = "0.01057"

- Modification time = "19/09/2019 11:36:27"

- Modification editor = "xrdpc2"

Delete Peak(s):

- Start position = "37.6343"

- End position = "37.7314"

- Modification time = "19/09/2019 11:36:53"

- Modification editor = "xrdpc2"

Delete Peak(s):

- Start position = "40.3379"

- End position = "40.3379"

- Modification time = "19/09/2019 11:37:12"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "40.458 - 46.266"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "12"

- Chi Square = "1.69537240057658"

- Rp = "0.02274"

- Rwp = "0.03056"

- Rexp = "0.01803"

- Modification time = "19/09/2019 11:37:27"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "47.283 - 53.091"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "8"

- Chi Square = "1.29488691147253"

- Rp = "0.02138"

- Rwp = "0.02847"

- Rexp = "0.02199"

- Modification time = "19/09/2019 11:37:46"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "52.4019"

- Modification time = "19/09/2019 11:37:50"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "50.484 - 59.163"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "20"

- Chi Square = "1.55694555797183"

- Rp = "0.02184"

- Rwp = "0.03073"

- Rexp = "0.01974"

- Modification time = "19/09/2019 11:38:09"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "53.6054"

- Modification time = "19/09/2019 11:38:12"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "50.484 - 59.163"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "24"

- Chi Square = "1.15282248273712"

- Rp = "0.01748"

- Rwp = "0.02257"

- Rexp = "0.01958"

- Modification time = "19/09/2019 11:38:17"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "58.998 - 67.677"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "12"

- Chi Square = "2.37594536217096"

- Rp = "0.02788"

- Rwp = "0.04496"

- Rexp = "0.01892"

- Modification time = "19/09/2019 11:38:28"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "60.6699"

- Modification time = "19/09/2019 11:38:29"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "58.998 - 67.677"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "16"

- Chi Square = "1.57885446261189"

- Rp = "0.02089"

- Rwp = "0.02964"

- Rexp = "0.01877"

- Modification time = "19/09/2019 11:38:34"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "66.495 - 69.960"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "4"

- Chi Square = "1.13727367474215"

- Rp = "0.01790"

- Rwp = "0.02202"

- Rexp = "0.01936"

- Modification time = "19/09/2019 11:38:49"

- Modification editor = "xrdpc2"

Search & Match:

- Allow pattern shift = "Yes"

- Auto residue = "Yes"

- Data source = "Profile and peak list"

- Demote unmatched strong = "No"

- Multi phase = "Yes"

- Restriction set = "Untitled"

- Restriction = "Restriction set"

- Subset name = ""

- Match intensity = "No"

- Two theta shift = "-0.3"

- Identify = "No"

- Max. no. of accepted patterns = "5"

- Minimum score = "50"

- Min. new lines / total lines = "60"

- Search depth = "10"

- Minimum new lines = "5"

- Minimum scale factor = "0.1"

- Intensity threshold = "0"

- Use line clustering = "Yes"

- Line cluster range = "1.5"

- Search sensitivity = "1.8"

- Use adaptive smoothing = "Yes"

- Smoothing range = "1.5"

- Threshold factor = "3"

- Match Threshold = "0"

- N * Esds = "-1"

- Raw Weight = "-1"

- Peak Shape = "-1"

- Accepted Shape = "-1"

- Peak Power = "-1"

- New Peak Power = "-1"

- Intensity Power = "-1"

- N Peaks Power = "-1"

- Modification time = "19/09/2019 10:20:20"

- Modification editor = "xrdpc2"