Fantastic report on

input.doc

Distribution:

| Name | Function | 0.1 | 0.5 | 1.0 |
| --- | --- | --- | --- | --- |
| N.N.-999 | Masterking Group Manager (MGM) |  |  |  |
| N.N.-998 | Product Ontwikkelt Manager (POM) |  |  |  |
| N.N.-1 | (AS) |  |  |  |
| N.N.-2 | (DS) |  |  |  |
| N.N.-3 | (BS) |  |  |  |
| T.P. | Supervisor All Coding |  |  |  |

# Table of Contents:

Table of Contents:	2

Anchor Scan Parameters: (Bookmark1)	3

Graphics: (Bookmark2)	4

Peak List: (Bookmark 3)	5

Identified Patterns List: (Bookmark4)	7

Plot of Identified Phases: (Bookmark 5)	7

Document History: (Bookmark 6)	8

# Anchor Scan Parameters: (Bookmark1)

Dataset Name	Ti3C2_1_20190722

File name	Y:\James Bird\Training\Ti3C2_1_20190722.xrdml

Sample Identification	1

Comment	Run by J E Warren sample queue batch

Configuration=Spinner, Owner=User-1, Creation date=08/12/2015 14:27:11

Goniometer=PW3050/60 (Theta/Theta); Minimum step size 2Theta:0.001; Minimum step size Omega:0.001

Sample stage=Spinner PW3064

Diffractometer system=XPERT-PRO

Measurement program=James Bird 10mm Mask, Owner=User-1, Creation date=22/07/2019 14:48:21

1h 5-70

Measurement Start Date/Time	22/07/2019 15:26:43

Operator	xrduser

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	5.0097

End Position [°2θ]	69.9537

Step Size [°2θ]	0.0330

Scan Step Time [s]	219.7100

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	2.12

Offset [°2θ]	0.0000

Divergence Slit Type	Automatic

Irradiated Length [mm]	8.00

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-Alpha1 [Å]	1.54060

K-Alpha2 [Å]	1.54443

K-Beta [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	40 mA, 40 kV

Diffractometer Type	0000000000007141

Diffractometer Number	0

Goniometer Radius [mm]	240.00

Dist. Focus-Diverg. Slit [mm]	100.00

Incident Beam Monochromator	No

Spinning	Yes

# Graphics: (Bookmark2)

# Peak List: (Bookmark 3)

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] | Tip Width | Matched by |
| --- | --- | --- | --- | --- | --- | --- |
| 5.7933 | 335.15 | 0.1000 | 15.24313 | 0.49 | 0.1200 |  |
| 5.8077 | 167.57 | 0.1000 | 15.24313 | 0.25 | 0.1200 |  |
| 5.9561 | 766.23 | 0.1000 | 14.82675 | 1.12 | 0.1200 |  |
| 5.9709 | 383.11 | 0.1000 | 14.82675 | 0.56 | 0.1200 |  |
| 6.1700 | 744.80 | 0.1000 | 14.31313 | 1.09 | 0.1200 |  |
| 6.1854 | 372.40 | 0.1000 | 14.31313 | 0.55 | 0.1200 |  |
| 6.3282 | 1504.42 | 0.1000 | 13.95571 | 2.20 | 0.1200 |  |
| 6.3439 | 752.21 | 0.1000 | 13.95571 | 1.10 | 0.1200 |  |
| 6.5154 | 2138.95 | 0.1000 | 13.55514 | 3.13 | 0.1200 |  |
| 6.5316 | 1069.48 | 0.1000 | 13.55514 | 1.57 | 0.1200 |  |
| 6.7116 | 2238.06 | 0.1000 | 13.15944 | 3.28 | 0.1200 |  |
| 6.7282 | 1119.03 | 0.1000 | 13.15944 | 1.64 | 0.1200 |  |
| 6.9531 | 571.55 | 0.1000 | 12.70284 | 0.84 | 0.1200 |  |
| 6.9704 | 285.77 | 0.1000 | 12.70284 | 0.42 | 0.1200 |  |
| 9.3362 | 9079.24 | 0.1000 | 9.46502 | 13.30 | 0.1200 |  |
| 9.3595 | 4539.62 | 0.1000 | 9.46502 | 6.65 | 0.1200 |  |
| 13.6666 | 406.52 | 0.1000 | 6.47411 | 0.60 | 0.1200 |  |
| 13.7008 | 203.26 | 0.1000 | 6.47411 | 0.30 | 0.1200 |  |
| 13.9168 | 226.69 | 0.1000 | 6.35828 | 0.33 | 0.1200 |  |
| 13.9516 | 113.35 | 0.1000 | 6.35828 | 0.17 | 0.1200 |  |
| 18.9242 | 4589.56 | 0.1000 | 4.68566 | 6.72 | 0.1200 | 00-052-0875 |
| 18.9716 | 2294.78 | 0.1000 | 4.68566 | 3.36 | 0.1200 |  |
| 25.4074 | 244.24 | 0.1000 | 3.50280 | 0.36 | 0.1200 |  |
| 25.4716 | 122.12 | 0.1000 | 3.50280 | 0.18 | 0.1200 |  |
| 28.1895 | 986.83 | 0.1000 | 3.16311 | 1.45 | 0.1200 |  |
| 28.2610 | 493.41 | 0.1000 | 3.16311 | 0.72 | 0.1200 |  |
| 28.4409 | 730.61 | 0.1000 | 3.13571 | 1.07 | 0.1200 |  |
| 28.5131 | 365.31 | 0.1000 | 3.13571 | 0.54 | 0.1200 |  |
| 28.6642 | 849.48 | 0.1000 | 3.11179 | 1.24 | 0.1200 |  |
| 28.7370 | 424.74 | 0.1000 | 3.11179 | 0.62 | 0.1200 |  |
| 33.8359 | 6444.13 | 0.1000 | 2.64706 | 9.44 | 0.1200 | 00-052-0875 |
| 33.9225 | 3222.07 | 0.1000 | 2.64706 | 4.72 | 0.1200 |  |
| 34.9819 | 1659.12 | 0.1000 | 2.56292 | 2.43 | 0.1200 |  |
| 35.0717 | 829.56 | 0.1000 | 2.56292 | 1.22 | 0.1200 |  |
| 35.7564 | 4595.62 | 0.1000 | 2.50916 | 6.73 | 0.1200 |  |
| 35.8482 | 2297.81 | 0.1000 | 2.50916 | 3.37 | 0.1200 |  |
| 36.5618 | 3188.87 | 0.1000 | 2.45571 | 4.67 | 0.1200 | 00-052-0875 |
| 36.6559 | 1594.43 | 0.1000 | 2.45571 | 2.34 | 0.1200 |  |
| 37.6646 | 446.72 | 0.1000 | 2.38631 | 0.65 | 0.1200 |  |
| 37.7618 | 223.36 | 0.1000 | 2.38631 | 0.33 | 0.1200 |  |
| 38.5866 | 68261.25 | 0.1000 | 2.33139 | 100.00 | 0.1200 | 00-052-0875 |
| 38.6863 | 34130.62 | 0.1000 | 2.33139 | 50.00 | 0.1200 |  |
| 38.8112 | 35819.82 | 0.1000 | 2.31841 | 52.47 | 0.1200 | 00-052-0875 |
| 38.9115 | 17909.91 | 0.1000 | 2.31841 | 26.24 | 0.1200 |  |
| 40.3002 | 446.30 | 0.1000 | 2.23611 | 0.65 | 0.1200 |  |
| 40.4047 | 223.15 | 0.1000 | 2.23611 | 0.33 | 0.1200 |  |
| 41.5530 | 22728.24 | 0.1000 | 2.17155 | 33.30 | 0.1200 | 00-052-0875 |
| 41.6611 | 11364.12 | 0.1000 | 2.17155 | 16.65 | 0.1200 |  |
| 43.2053 | 1270.18 | 0.1000 | 2.09225 | 1.86 | 0.1200 |  |
| 43.3181 | 635.09 | 0.1000 | 2.09225 | 0.93 | 0.1200 |  |
| 44.7225 | 1525.95 | 0.1000 | 2.02473 | 2.24 | 0.1200 | 00-052-0875 |
| 44.8396 | 762.97 | 0.1000 | 2.02473 | 1.12 | 0.1200 |  |
| 48.2472 | 6222.21 | 0.1000 | 1.88472 | 9.12 | 0.1200 | 00-052-0875 |
| 48.3748 | 3111.10 | 0.1000 | 1.88472 | 4.56 | 0.1200 |  |
| 52.0813 | 2742.52 | 0.1000 | 1.75463 | 4.02 | 0.1200 | 00-052-0875 |
| 52.2205 | 1371.26 | 0.1000 | 1.75463 | 2.01 | 0.1200 |  |
| 52.4051 | 577.52 | 0.1000 | 1.74455 | 0.85 | 0.1200 |  |
| 52.5452 | 288.76 | 0.1000 | 1.74455 | 0.42 | 0.1200 |  |
| 52.8414 | 178.00 | 0.1000 | 1.73117 | 0.26 | 0.1200 |  |
| 52.9829 | 89.00 | 0.1000 | 1.73117 | 0.13 | 0.1200 |  |
| 56.2183 | 11713.10 | 0.1000 | 1.63492 | 17.16 | 0.1200 | 00-052-0875 |
| 56.3704 | 5856.55 | 0.1000 | 1.63492 | 8.58 | 0.1200 |  |
| 57.3645 | 1888.51 | 0.1000 | 1.60495 | 2.77 | 0.1200 |  |
| 57.5203 | 944.25 | 0.1000 | 1.60495 | 1.38 | 0.1200 |  |
| 60.0185 | 13353.86 | 0.1000 | 1.54017 | 19.56 | 0.1200 | 00-052-0875 |
| 60.1830 | 6676.93 | 0.1000 | 1.54017 | 9.78 | 0.1200 |  |
| 60.3120 | 5938.10 | 0.1000 | 1.53337 | 8.70 | 0.1200 |  |
| 60.4775 | 2969.05 | 0.1000 | 1.53337 | 4.35 | 0.1200 |  |
| 60.7034 | 3109.32 | 0.1000 | 1.52442 | 4.56 | 0.1200 | 00-052-0875 |
| 60.8702 | 1554.66 | 0.1000 | 1.52442 | 2.28 | 0.1200 |  |
| 61.1326 | 960.00 | 0.1000 | 1.51474 | 1.41 | 0.1200 |  |
| 61.3009 | 480.00 | 0.1000 | 1.51474 | 0.70 | 0.1200 |  |
| 63.6017 | 402.45 | 0.1000 | 1.46175 | 0.59 | 0.1200 |  |
| 63.7784 | 201.23 | 0.1000 | 1.46175 | 0.29 | 0.1200 |  |
| 65.2603 | 6181.03 | 0.1000 | 1.42856 | 9.05 | 0.1200 | 00-052-0875 |
| 65.4427 | 3090.51 | 0.1000 | 1.42856 | 4.53 | 0.1200 |  |
| 66.3865 | 476.33 | 0.1000 | 1.40703 | 0.70 | 0.1200 |  |
| 66.5729 | 238.17 | 0.1000 | 1.40703 | 0.35 | 0.1200 |  |
| 68.0789 | 783.37 | 0.1000 | 1.37611 | 1.15 | 0.1200 |  |
| 68.2714 | 391.69 | 0.1000 | 1.37611 | 0.57 | 0.1200 |  |

# Identified Patterns List: (Bookmark4)

| Visible | Ref.Code | Score | Compound Name | Displ.[°2θ] | Scale Fac. | Chem. Formula |
| --- | --- | --- | --- | --- | --- | --- |
| * | 00-052-0875 | 36 | Aluminum Titanium Carbide | -0.300 | 0.440 | Ti3 Al C2 |
| * | 00-046-1212 | 6 | Aluminum Oxide | -0.300 | 0.011 | Al2 O3 |

# Plot of Identified Phases: (Bookmark 5)

# Document History: (Bookmark 6)

Beam attenuation factor(s) used to back-calculate ESDs:

- Modification time = "19/09/2019 09:34:28"

- Modification editor = "xrdpc2"

Insert Measurement:

- File name = "Ti3C2_1_20190722.xrdml"

- Modification time = "19/09/2019 09:34:28"

- Modification editor = "xrdpc2"

Default properties:

- Measurement step axis = "None"

- Internal wavelengths used from anode material: Copper (Cu)

- Original K-Alpha1 wavelength = "1.54060"

- Used K-Alpha1 wavelength = "1.54060"

- Original K-Alpha2 wavelength = "1.54443"

- Used K-Alpha2 wavelength = "1.54443"

- Original K-Beta wavelength = "1.39225"

- Used K-Beta wavelength = "1.39225"

- Fixed div. slit size = "1.00000"

- Receiving slit size = "0.10000"

- Step axis value = "0.00000"

- Offset = "0.00000"

- Sample length = "10.00000"

- Modification time = "19/09/2019 09:34:28"

- Modification editor = "xrdpc2"

Interpolate Step Size:

- Initial Scan Range = 5.00971 - 69.98310

- Initial Step Size = 0.03342

- Derived Step Size = 0.03300

- Use Derived Step Size = "Yes"

- Modification time = "19/09/2019 09:34:28"

- Modification editor = "PANalytical"

Take As Anchor Scan:

- Scan name = "Ti3C2_1_20190722"

- Modification time = "19/09/2019 09:41:27"

- Modification editor = "xrdpc2"

Take As Anchor Scan:

- Scan name = "Ti3C2_1_20190722"

- Modification time = "19/09/2019 09:41:31"

- Modification editor = "xrdpc2"

Take As Anchor Scan:

- Scan name = "Ti3C2_1_20190722"

- Modification time = "19/09/2019 09:50:30"

- Modification editor = "xrdpc2"

Take As Anchor Scan:

- Scan name = "Ti3C2_1_20190722"

- Modification time = "19/09/2019 09:57:47"

- Modification editor = "xrdpc2"

Determine Background:

- Add to net scan = "Nothing"

- User defined intensity = "-5"

- Correction method = "Automatic"

- Bending factor = "5"

- Minimum significance = "0.7"

- Minimum tip width = "0"

- Maximum tip width = "1"

- Peak base width = "2"

- Use smoothed input data = "Yes"

- Granularity = "20"

- Modification time = "22/02/2001 10:17:43"

- Modification editor = "PANalytical"

Take As Anchor Scan:

- Scan name = "Ti3C2_1_20190722"

- Modification time = "19/09/2019 11:12:24"

- Modification editor = "xrdpc2"

Search Peaks:

- Minimum significance = "1"

- Minimum tip width = "0.01"

- Maximum tip width = "1"

- Peak base width = "2"

- Method = "Minimum 2nd derivative"

- Modification time = "19/09/2019 11:12:35"

- Modification editor = "PANalytical"

Insert Peak:

- Peak position Gonio = "60.2856"

- Modification time = "19/09/2019 11:13:10"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "59.202 - 61.842"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "8"

- Chi Square = "13.5545782733438"

- Rp = "0.14274"

- Rwp = "0.19075"

- Rexp = "0.01407"

- Modification time = "19/09/2019 11:13:22"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "60.7143"

- Modification time = "19/09/2019 11:13:51"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "59.202 - 61.842"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "12"

- Chi Square = "7.60354907946379"

- Rp = "0.08240"

- Rwp = "0.10399"

- Rexp = "0.01368"

- Modification time = "19/09/2019 11:13:57"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "61.1846"

- Modification time = "19/09/2019 11:14:11"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "59.202 - 61.842"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "16"

- Chi Square = "6.88145706681263"

- Rp = "0.07211"

- Rwp = "0.09130"

- Rexp = "0.01327"

- Modification time = "19/09/2019 11:14:15"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "5.010 - 11.643"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "8"

- Chi Square = "9.60259890678061"

- Rp = "0.11386"

- Rwp = "0.18415"

- Rexp = "0.01918"

- Modification time = "19/09/2019 11:14:37"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "6.5515"

- Modification time = "19/09/2019 11:14:43"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "6.3827"

- Modification time = "19/09/2019 11:14:45"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "5.8235"

- Modification time = "19/09/2019 11:14:48"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "5.010 - 11.643"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "20"

- Chi Square = "4.28996819466005"

- Rp = "0.05767"

- Rwp = "0.07968"

- Rexp = "0.01857"

- BCLM Exit Code = "Refinement iterations exceeded"

- Modification time = "19/09/2019 11:14:57"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "6.1822"

- Modification time = "19/09/2019 11:15:00"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "5.010 - 11.643"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "24"

- Chi Square = "3.81270992251654"

- Rp = "0.05217"

- Rwp = "0.07004"

- Rexp = "0.01837"

- Modification time = "19/09/2019 11:15:05"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "6.9840"

- Modification time = "19/09/2019 11:15:09"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "5.010 - 11.643"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "28"

- Chi Square = "3.34700401537969"

- Rp = "0.04597"

- Rwp = "0.06079"

- Rexp = "0.01816"

- Modification time = "19/09/2019 11:15:13"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "5.8129"

- Modification time = "19/09/2019 11:15:32"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "5.010 - 11.643"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "32"

- Chi Square = "3.18592734336211"

- Rp = "0.04266"

- Rwp = "0.05719"

- Rexp = "0.01795"

- Modification time = "19/09/2019 11:15:36"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "10.818 - 17.451"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "8"

- Chi Square = "1.49958756404273"

- Rp = "0.02458"

- Rwp = "0.03446"

- Rexp = "0.02298"

- Modification time = "19/09/2019 11:15:50"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "13.9104"

- Modification time = "19/09/2019 11:15:56"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "10.818 - 17.451"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "12"

- Chi Square = "1.20499714390601"

- Rp = "0.02088"

- Rwp = "0.02740"

- Rexp = "0.02274"

- Modification time = "19/09/2019 11:16:00"

- Modification editor = "xrdpc2"

Delete Peak(s):

- Start position = "12.7465"

- End position = "12.7783"

- Modification time = "19/09/2019 11:16:29"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "17.0080"

- Modification time = "19/09/2019 11:16:37"

- Modification editor = "xrdpc2"

Delete Peak(s):

- Start position = "17.0079"

- End position = "17.0079"

- Modification time = "19/09/2019 11:16:51"

- Modification editor = "xrdpc2"

Delete Peak(s):

- Start position = "17.8819"

- End position = "17.8819"

- Modification time = "19/09/2019 11:17:00"

- Modification editor = "xrdpc2"

Delete Peak(s):

- Start position = "20.9821"

- End position = "20.9821"

- Modification time = "19/09/2019 11:17:19"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "15.279 - 20.328"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "4"

- Chi Square = "1.51693517938617"

- Rp = "0.02659"

- Rwp = "0.03347"

- Rexp = "0.02207"

- Modification time = "19/09/2019 11:17:29"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "24.876 - 29.925"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "12"

- Chi Square = "3.44917884060015"

- Rp = "0.05399"

- Rwp = "0.07545"

- Rexp = "0.02187"

- Modification time = "19/09/2019 11:17:40"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "26.895 - 29.304"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "8"

- Chi Square = "4.93540044651173"

- Rp = "0.08177"

- Rwp = "0.09841"

- Rexp = "0.01994"

- Modification time = "19/09/2019 11:17:50"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "28.4512"

- Modification time = "19/09/2019 11:17:55"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "26.895 - 29.304"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "12"

- Chi Square = "4.1264182149447"

- Rp = "0.06290"

- Rwp = "0.07971"

- Rexp = "0.01932"

- Modification time = "19/09/2019 11:18:01"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "33.126 - 34.512"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "4"

- Chi Square = "2.04471691574828"

- Rp = "0.03156"

- Rwp = "0.03705"

- Rexp = "0.01812"

- Modification time = "19/09/2019 11:18:22"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "34.551 - 42.537"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "32"

- Chi Square = "7.83433409631835"

- Rp = "0.06784"

- Rwp = "0.09129"

- Rexp = "0.01165"

- Modification time = "19/09/2019 11:18:46"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "42.432 - 50.418"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "12"

- Chi Square = "2.1845769702873"

- Rp = "0.03100"

- Rwp = "0.04537"

- Rexp = "0.02077"

- Modification time = "19/09/2019 11:18:58"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "50.979 - 58.965"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "20"

- Chi Square = "3.69467492652978"

- Rp = "0.05357"

- Rwp = "0.07386"

- Rexp = "0.01999"

- Modification time = "19/09/2019 11:19:08"

- Modification editor = "xrdpc2"

Delete Peak(s):

- Start position = "54.2109"

- End position = "54.2109"

- Modification time = "19/09/2019 11:19:20"

- Modification editor = "xrdpc2"

Delete Peak(s):

- Start position = "54.0655"

- End position = "54.0655"

- Modification time = "19/09/2019 11:19:26"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "52.3825"

- Modification time = "19/09/2019 11:19:49"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "51.183 - 53.856"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "12"

- Chi Square = "2.2986639261988"

- Rp = "0.03800"

- Rwp = "0.04940"

- Rexp = "0.02149"

- Modification time = "19/09/2019 11:19:55"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "55.434 - 58.107"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "8"

- Chi Square = "5.4955950469196"

- Rp = "0.07488"

- Rwp = "0.09180"

- Rexp = "0.01670"

- Modification time = "19/09/2019 11:20:12"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "59.394 - 62.067"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "16"

- Chi Square = "6.65831845190026"

- Rp = "0.07139"

- Rwp = "0.08923"

- Rexp = "0.01340"

- Modification time = "19/09/2019 11:20:23"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "62.469 - 69.960"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "16"

- Chi Square = "9.29213723038015"

- Rp = "0.08645"

- Rwp = "0.18521"

- Rexp = "0.01993"

- Modification time = "19/09/2019 11:20:42"

- Modification editor = "xrdpc2"

Search & Match:

- Allow pattern shift = "Yes"

- Auto residue = "Yes"

- Data source = "Profile and peak list"

- Demote unmatched strong = "No"

- Multi phase = "Yes"

- Restriction set = "Untitled"

- Restriction = "Restriction set"

- Subset name = ""

- Match intensity = "No"

- Two theta shift = "-0.3"

- Identify = "No"

- Max. no. of accepted patterns = "5"

- Minimum score = "50"

- Min. new lines / total lines = "60"

- Search depth = "10"

- Minimum new lines = "5"

- Minimum scale factor = "0.1"

- Intensity threshold = "0"

- Use line clustering = "Yes"

- Line cluster range = "1.5"

- Search sensitivity = "1.8"

- Use adaptive smoothing = "Yes"

- Smoothing range = "1.5"

- Threshold factor = "3"

- Match Threshold = "0"

- N * Esds = "-1"

- Raw Weight = "-1"

- Peak Shape = "-1"

- Accepted Shape = "-1"

- Peak Power = "-1"

- New Peak Power = "-1"

- Intensity Power = "-1"

- N Peaks Power = "-1"

- Modification time = "19/09/2019 10:20:20"

- Modification editor = "xrdpc2"