Fantastic report on

input.doc

Distribution:

| Name | Function | 0.1 | 0.5 | 1.0 |
| --- | --- | --- | --- | --- |
| N.N.-999 | Masterking Group Manager (MGM) |  |  |  |
| N.N.-998 | Product Ontwikkelt Manager (POM) |  |  |  |
| N.N.-1 | (AS) |  |  |  |
| N.N.-2 | (DS) |  |  |  |
| N.N.-3 | (BS) |  |  |  |
| T.P. | Supervisor All Coding |  |  |  |

# Table of Contents:

Table of Contents:	2

Anchor Scan Parameters: (Bookmark1)	3

Graphics: (Bookmark2)	4

Peak List: (Bookmark 3)	5

Identified Patterns List: (Bookmark4)	7

Plot of Identified Phases: (Bookmark 5)	7

Document History: (Bookmark 6)	8

# Anchor Scan Parameters: (Bookmark1)

Dataset Name	Ti3C2_3_20190722

File name	Y:\James Bird\Training\Ti3C2_3_20190722.xrdml

Sample Identification	3

Comment	Run by J E Warren sample queue batch

Configuration=Spinner, Owner=User-1, Creation date=08/12/2015 14:27:11

Goniometer=PW3050/60 (Theta/Theta); Minimum step size 2Theta:0.001; Minimum step size Omega:0.001

Sample stage=Spinner PW3064

Diffractometer system=XPERT-PRO

Measurement program=James Bird 10mm Mask, Owner=User-1, Creation date=22/07/2019 14:48:21

1h 5-70

Measurement Start Date/Time	22/07/2019 17:48:36

Operator	xrduser

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	5.0097

End Position [°2θ]	69.9537

Step Size [°2θ]	0.0330

Scan Step Time [s]	219.7100

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	2.12

Offset [°2θ]	0.0000

Divergence Slit Type	Automatic

Irradiated Length [mm]	8.00

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-Alpha1 [Å]	1.54060

K-Alpha2 [Å]	1.54443

K-Beta [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	40 mA, 40 kV

Diffractometer Type	0000000000007141

Diffractometer Number	0

Goniometer Radius [mm]	240.00

Dist. Focus-Diverg. Slit [mm]	100.00

Incident Beam Monochromator	No

Spinning	Yes

# Graphics: (Bookmark2)

# Peak List: (Bookmark 3)

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] | Tip Width | Matched by |
| --- | --- | --- | --- | --- | --- | --- |
| 6.8916 | 78791.87 | 0.1000 | 12.81597 | 94.49 | 0.1200 |  |
| 6.9088 | 39395.93 | 0.1000 | 12.81597 | 47.25 | 0.1200 |  |
| 9.5234 | 20946.55 | 0.1000 | 9.27938 | 25.12 | 0.1200 | 04-012-0632 |
| 9.5471 | 10473.28 | 0.1000 | 9.27938 | 12.56 | 0.1200 |  |
| 13.8267 | 3981.34 | 0.1000 | 6.39952 | 4.77 | 0.1200 |  |
| 13.8612 | 1990.67 | 0.1000 | 6.39952 | 2.39 | 0.1200 |  |
| 14.0700 | 4143.74 | 0.1000 | 6.28941 | 4.97 | 0.1200 |  |
| 14.1051 | 2071.87 | 0.1000 | 6.28941 | 2.48 | 0.1200 |  |
| 19.1092 | 6688.17 | 0.1000 | 4.64070 | 8.02 | 0.1200 | 04-012-0632 |
| 19.1572 | 3344.08 | 0.1000 | 4.64070 | 4.01 | 0.1200 |  |
| 20.8351 | 1214.67 | 0.1000 | 4.26001 | 1.46 | 0.1200 |  |
| 20.8875 | 607.33 | 0.1000 | 4.26001 | 0.73 | 0.1200 |  |
| 27.1700 | 3258.13 | 0.1000 | 3.27944 | 3.91 | 0.1200 | 04-003-0648 |
| 27.2388 | 1629.06 | 0.1000 | 3.27944 | 1.95 | 0.1200 |  |
| 27.5083 | 3660.11 | 0.1000 | 3.23987 | 4.39 | 0.1200 |  |
| 27.5780 | 1830.06 | 0.1000 | 3.23987 | 2.19 | 0.1200 |  |
| 28.4760 | 8583.96 | 0.1000 | 3.13192 | 10.29 | 0.1200 |  |
| 28.5483 | 4291.98 | 0.1000 | 3.13192 | 5.15 | 0.1200 |  |
| 28.8362 | 5931.78 | 0.1000 | 3.09362 | 7.11 | 0.1200 | 04-012-0632 |
| 28.9095 | 2965.89 | 0.1000 | 3.09362 | 3.56 | 0.1200 |  |
| 34.0039 | 2279.60 | 0.1000 | 2.63437 | 2.73 | 0.1200 | 04-012-0632 |
| 34.0909 | 1139.80 | 0.1000 | 2.63437 | 1.37 | 0.1200 |  |
| 35.1506 | 3493.68 | 0.1000 | 2.55101 | 4.19 | 0.1200 | 00-046-1212 |
| 35.2408 | 1746.84 | 0.1000 | 2.55101 | 2.09 | 0.1200 |  |
| 35.9176 | 7095.64 | 0.1000 | 2.49827 | 8.51 | 0.1200 | 04-004-2919, 04-003-0648 |
| 36.0099 | 3547.82 | 0.1000 | 2.49827 | 4.25 | 0.1200 |  |
| 36.7346 | 1904.06 | 0.1000 | 2.44456 | 2.28 | 0.1200 | 04-012-0632 |
| 36.8291 | 952.03 | 0.1000 | 2.44456 | 1.14 | 0.1200 |  |
| 38.7847 | 83386.11 | 0.1000 | 2.31993 | 100.00 | 0.1200 | 04-012-0632 |
| 38.8849 | 41693.06 | 0.1000 | 2.31993 | 50.00 | 0.1200 |  |
| 40.4457 | 293.19 | 0.1000 | 2.22841 | 0.35 | 0.1200 |  |
| 40.5506 | 146.60 | 0.1000 | 2.22841 | 0.18 | 0.1200 |  |
| 41.7133 | 12743.12 | 0.1000 | 2.16357 | 15.28 | 0.1200 | 04-004-2919, 00-046-1212, 04-012-0632 |
| 41.8218 | 6371.56 | 0.1000 | 2.16357 | 7.64 | 0.1200 |  |
| 43.3578 | 3576.45 | 0.1000 | 2.08524 | 4.29 | 0.1200 | 00-046-1212 |
| 43.4710 | 1788.22 | 0.1000 | 2.08524 | 2.14 | 0.1200 |  |
| 44.9034 | 408.23 | 0.1000 | 2.01699 | 0.49 | 0.1200 | 04-012-0632 |
| 45.0211 | 204.12 | 0.1000 | 2.01699 | 0.24 | 0.1200 |  |
| 48.4366 | 1796.79 | 0.1000 | 1.87780 | 2.15 | 0.1200 | 04-012-0632 |
| 48.5647 | 898.39 | 0.1000 | 1.87780 | 1.08 | 0.1200 |  |
| 52.2836 | 774.80 | 0.1000 | 1.74832 | 0.93 | 0.1200 | 04-012-0632 |
| 52.4234 | 387.40 | 0.1000 | 1.74832 | 0.46 | 0.1200 |  |
| 53.9485 | 542.15 | 0.1000 | 1.69823 | 0.65 | 0.1200 | 04-003-0648 |
| 54.0934 | 271.08 | 0.1000 | 1.69823 | 0.33 | 0.1200 |  |
| 56.4102 | 3201.79 | 0.1000 | 1.62982 | 3.84 | 0.1200 | 04-012-0632, 04-003-0648 |
| 56.5629 | 1600.90 | 0.1000 | 1.62982 | 1.92 | 0.1200 |  |
| 57.5037 | 1138.31 | 0.1000 | 1.60140 | 1.37 | 0.1200 | 00-046-1212 |
| 57.6600 | 569.16 | 0.1000 | 1.60140 | 0.68 | 0.1200 |  |
| 60.1946 | 2873.23 | 0.1000 | 1.53608 | 3.45 | 0.1200 | 04-012-0632 |
| 60.3597 | 1436.62 | 0.1000 | 1.53608 | 1.72 | 0.1200 |  |
| 60.4453 | 2380.67 | 0.1000 | 1.53031 | 2.85 | 0.1200 | 04-004-2919 |
| 60.6112 | 1190.33 | 0.1000 | 1.53031 | 1.43 | 0.1200 |  |
| 60.9650 | 1015.88 | 0.1000 | 1.51850 | 1.22 | 0.1200 | 04-012-0632 |
| 61.1326 | 507.94 | 0.1000 | 1.51850 | 0.61 | 0.1200 |  |
| 65.4562 | 1577.90 | 0.1000 | 1.42476 | 1.89 | 0.1200 | 04-012-0632 |
| 65.6392 | 788.95 | 0.1000 | 1.42476 | 0.95 | 0.1200 |  |
| 66.6703 | 310.02 | 0.1000 | 1.40173 | 0.37 | 0.1200 |  |
| 66.8577 | 155.01 | 0.1000 | 1.40173 | 0.19 | 0.1200 |  |
| 68.1938 | 587.32 | 0.1000 | 1.37408 | 0.70 | 0.1200 | 00-046-1212 |
| 68.3867 | 293.66 | 0.1000 | 1.37408 | 0.35 | 0.1200 |  |

# Identified Patterns List: (Bookmark4)

| Visible | Ref.Code | Score | Compound Name | Displ.[°2θ] | Scale Fac. | Chem. Formula |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-004-2919 | 38 | Titanium Carbide | -0.054 | 0.055 | Ti C |
| * | 00-046-1212 | 33 | Aluminum Oxide | -0.048 | 0.022 | Al2 O3 |
| * | 04-012-0632 | 31 | Titanium Aluminum Carbide | -0.072 | 0.244 | Ti3 Al C2 |
| * | 04-003-0648 | 15 | Titanium Oxide | -0.271 | 0.035 | Ti O2 |

# Plot of Identified Phases: (Bookmark 5)

# Document History: (Bookmark 6)

Beam attenuation factor(s) used to back-calculate ESDs:

- Modification time = "19/09/2019 09:34:28"

- Modification editor = "xrdpc2"

Insert Measurement:

- File name = "Ti3C2_3_20190722.xrdml"

- Modification time = "19/09/2019 09:34:28"

- Modification editor = "xrdpc2"

Default properties:

- Measurement step axis = "None"

- Internal wavelengths used from anode material: Copper (Cu)

- Original K-Alpha1 wavelength = "1.54060"

- Used K-Alpha1 wavelength = "1.54060"

- Original K-Alpha2 wavelength = "1.54443"

- Used K-Alpha2 wavelength = "1.54443"

- Original K-Beta wavelength = "1.39225"

- Used K-Beta wavelength = "1.39225"

- Fixed div. slit size = "1.00000"

- Receiving slit size = "0.10000"

- Step axis value = "0.00000"

- Offset = "0.00000"

- Sample length = "10.00000"

- Modification time = "19/09/2019 09:34:28"

- Modification editor = "xrdpc2"

Interpolate Step Size:

- Initial Scan Range = 5.00971 - 69.98310

- Initial Step Size = 0.03342

- Derived Step Size = 0.03300

- Use Derived Step Size = "Yes"

- Modification time = "19/09/2019 09:34:28"

- Modification editor = "PANalytical"

Take As Anchor Scan:

- Scan name = "Ti3C2_3_20190722"

- Modification time = "19/09/2019 09:41:33"

- Modification editor = "xrdpc2"

Take As Anchor Scan:

- Scan name = "Ti3C2_3_20190722"

- Modification time = "19/09/2019 09:50:31"

- Modification editor = "xrdpc2"

Take As Anchor Scan:

- Scan name = "Ti3C2_3_20190722"

- Modification time = "19/09/2019 09:58:28"

- Modification editor = "xrdpc2"

Determine Background:

- Add to net scan = "Nothing"

- User defined intensity = "-5"

- Correction method = "Automatic"

- Bending factor = "5"

- Minimum significance = "0.7"

- Minimum tip width = "0"

- Maximum tip width = "1"

- Peak base width = "2"

- Use smoothed input data = "Yes"

- Granularity = "20"

- Modification time = "22/02/2001 10:17:43"

- Modification editor = "PANalytical"

Take As Anchor Scan:

- Scan name = "Ti3C2_3_20190722"

- Modification time = "19/09/2019 11:45:01"

- Modification editor = "xrdpc2"

Search Peaks:

- Minimum significance = "1"

- Minimum tip width = "0.01"

- Maximum tip width = "1"

- Peak base width = "2"

- Method = "Minimum 2nd derivative"

- Modification time = "19/09/2019 11:45:16"

- Modification editor = "PANalytical"

Profile/Rietveld fitting:

- Angular range Gonio = "5.010 - 11.445"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "8"

- Chi Square = "56.1796717982982"

- Rp = "0.41370"

- Rwp = "0.49562"

- Rexp = "0.00882"

- Modification time = "19/09/2019 11:45:45"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "5.010 - 11.445"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "8"

- Chi Square = "56.1184601517273"

- Rp = "0.41337"

- Rwp = "0.49508"

- Rexp = "0.00882"

- Modification time = "19/09/2019 11:46:54"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "11.577 - 18.012"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "8"

- Chi Square = "8.75882967985312"

- Rp = "0.09959"

- Rwp = "0.14811"

- Rexp = "0.01691"

- Modification time = "19/09/2019 11:47:06"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "17.418 - 23.853"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "8"

- Chi Square = "3.42453050801518"

- Rp = "0.04461"

- Rwp = "0.06142"

- Rexp = "0.01793"

- Modification time = "19/09/2019 11:47:16"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "23.430 - 32.109"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "16"

- Chi Square = "15.508395926366"

- Rp = "0.15874"

- Rwp = "0.22595"

- Rexp = "0.01457"

- Modification time = "19/09/2019 11:47:51"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "27.4766"

- Modification time = "19/09/2019 11:48:02"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "23.430 - 32.109"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "20"

- Chi Square = "14.1059421348871"

- Rp = "0.14196"

- Rwp = "0.20385"

- Rexp = "0.01445"

- Modification time = "19/09/2019 11:48:09"

- Modification editor = "xrdpc2"

Delete Peak(s):

- Start position = "25.5656"

- End position = "25.6302"

- Modification time = "19/09/2019 11:48:50"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "32.010 - 37.587"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "16"

- Chi Square = "9.55489472971247"

- Rp = "0.09834"

- Rwp = "0.13767"

- Rexp = "0.01441"

- Modification time = "19/09/2019 11:49:04"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "37.515 - 43.092"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "12"

- Chi Square = "10.1507637071655"

- Rp = "0.08515"

- Rwp = "0.10962"

- Rexp = "0.01080"

- Modification time = "19/09/2019 11:49:14"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "40.584 - 46.161"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "12"

- Chi Square = "7.16176527662959"

- Rp = "0.07230"

- Rwp = "0.10051"

- Rexp = "0.01403"

- Modification time = "19/09/2019 11:49:27"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "47.283 - 57.084"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "16"

- Chi Square = "1.74872501861958"

- Rp = "0.02674"

- Rwp = "0.03519"

- Rexp = "0.02013"

- Modification time = "19/09/2019 11:50:12"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "54.840 - 64.641"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "16"

- Chi Square = "2.7992579108469"

- Rp = "0.02986"

- Rwp = "0.04769"

- Rexp = "0.01704"

- Modification time = "19/09/2019 11:50:22"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "60.9840"

- Modification time = "19/09/2019 11:50:27"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "54.840 - 64.641"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "20"

- Chi Square = "1.95481224693507"

- Rp = "0.02321"

- Rwp = "0.03306"

- Rexp = "0.01691"

- Modification time = "19/09/2019 11:50:34"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "63.492 - 69.597"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "12"

- Chi Square = "1.32323940483093"

- Rp = "0.01866"

- Rwp = "0.02330"

- Rexp = "0.01761"

- Modification time = "19/09/2019 11:50:45"

- Modification editor = "xrdpc2"

Search & Match:

- Allow pattern shift = "Yes"

- Auto residue = "Yes"

- Data source = "Profile and peak list"

- Demote unmatched strong = "No"

- Multi phase = "Yes"

- Restriction set = "Untitled"

- Restriction = "Restriction set"

- Subset name = ""

- Match intensity = "No"

- Two theta shift = "-0.3"

- Identify = "No"

- Max. no. of accepted patterns = "5"

- Minimum score = "50"

- Min. new lines / total lines = "60"

- Search depth = "10"

- Minimum new lines = "5"

- Minimum scale factor = "0.1"

- Intensity threshold = "0"

- Use line clustering = "Yes"

- Line cluster range = "1.5"

- Search sensitivity = "1.8"

- Use adaptive smoothing = "Yes"

- Smoothing range = "1.5"

- Threshold factor = "3"

- Match Threshold = "0"

- N * Esds = "-1"

- Raw Weight = "-1"

- Peak Shape = "-1"

- Accepted Shape = "-1"

- Peak Power = "-1"

- New Peak Power = "-1"

- Intensity Power = "-1"

- N Peaks Power = "-1"

- Modification time = "19/09/2019 10:20:20"

- Modification editor = "xrdpc2"