Fantastic report on

input.doc

Distribution:

| Name | Function | 0.1 | 0.5 | 1.0 |
| --- | --- | --- | --- | --- |
| N.N.-999 | Masterking Group Manager (MGM) |  |  |  |
| N.N.-998 | Product Ontwikkelt Manager (POM) |  |  |  |
| N.N.-1 | (AS) |  |  |  |
| N.N.-2 | (DS) |  |  |  |
| N.N.-3 | (BS) |  |  |  |
| T.P. | Supervisor All Coding |  |  |  |

# Table of Contents:

Table of Contents:	2

Anchor Scan Parameters: (Bookmark1)	3

Graphics: (Bookmark2)	4

Peak List: (Bookmark 3)	5

Identified Patterns List: (Bookmark4)	7

Plot of Identified Phases: (Bookmark 5)	7

Document History: (Bookmark 6)	8

# Anchor Scan Parameters: (Bookmark1)

Dataset Name	Ti3AlC2_30-08_20190918

File name	Y:\James Bird\Training\Ti3AlC2 or Ti3C2Tx\Ti3AlC2_30-08_20190918.xrdml

Sample Identification	30-08

Comment	Configuration=Spinner, Owner=User-1, Creation date=08/12/2015 14:27:11

Goniometer=PW3050/60 (Theta/Theta); Minimum step size 2Theta:0.001; Minimum step size Omega:0.001

Sample stage=Spinner PW3064

Diffractometer system=XPERT-PRO

Measurement program=James Bird 10mm Mask Refinement, Owner=User-1, Creation date=18/09/2019 16:54:35

Refinement

Measurement Start Date/Time	18/09/2019 21:34:56

Operator	xrduser

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	5.0014

End Position [°2θ]	69.9754

Step Size [°2θ]	0.0170

Scan Step Time [s]	514.9850

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	2.12

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.2500

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-Alpha1 [Å]	1.54060

K-Alpha2 [Å]	1.54443

K-Beta [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	40 mA, 40 kV

Diffractometer Type	0000000000007141

Diffractometer Number	0

Goniometer Radius [mm]	240.00

Dist. Focus-Diverg. Slit [mm]	100.00

Incident Beam Monochromator	No

Spinning	Yes

# Graphics: (Bookmark2)

# Peak List: (Bookmark 3)

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] | Tip Width | Matched by |
| --- | --- | --- | --- | --- | --- | --- |
| 6.8119 | 34690.31 | 0.1000 | 12.96587 | 68.75 | 0.1200 |  |
| 6.8288 | 17345.15 | 0.1000 | 12.96587 | 34.37 | 0.1200 |  |
| 9.4426 | 29473.19 | 0.1000 | 9.35861 | 58.41 | 0.1200 | 04-012-0632 |
| 9.4661 | 14736.60 | 0.1000 | 9.35861 | 29.20 | 0.1200 |  |
| 12.8731 | 292.02 | 0.1000 | 6.87134 | 0.58 | 0.1200 |  |
| 12.9053 | 146.01 | 0.1000 | 6.87134 | 0.29 | 0.1200 |  |
| 13.9341 | 1503.19 | 0.1000 | 6.35046 | 2.98 | 0.1200 |  |
| 13.9688 | 751.60 | 0.1000 | 6.35046 | 1.49 | 0.1200 |  |
| 19.0378 | 4706.31 | 0.1000 | 4.65796 | 9.33 | 0.1200 | 04-012-0632 |
| 19.0855 | 2353.15 | 0.1000 | 4.65796 | 4.66 | 0.1200 |  |
| 25.5033 | 620.94 | 0.1000 | 3.48985 | 1.23 | 0.1200 | 04-004-2852 |
| 25.5677 | 310.47 | 0.1000 | 3.48985 | 0.62 | 0.1200 |  |
| 28.7659 | 1543.63 | 0.1000 | 3.10102 | 3.06 | 0.1200 | 04-012-0632 |
| 28.8389 | 771.82 | 0.1000 | 3.10102 | 1.53 | 0.1200 |  |
| 33.6408 | 71.62 | 0.1000 | 2.66196 | 0.14 | 0.1200 |  |
| 33.7269 | 35.81 | 0.1000 | 2.66196 | 0.07 | 0.1200 |  |
| 33.9428 | 11799.43 | 0.1000 | 2.63896 | 23.38 | 0.1200 | 04-012-0632 |
| 34.0297 | 5899.71 | 0.1000 | 2.63896 | 11.69 | 0.1200 |  |
| 35.0637 | 2478.12 | 0.1000 | 2.55713 | 4.91 | 0.1200 | 04-004-2852 |
| 35.1537 | 1239.06 | 0.1000 | 2.55713 | 2.46 | 0.1200 |  |
| 35.8481 | 4028.83 | 0.1000 | 2.50296 | 7.98 | 0.1200 |  |
| 35.9402 | 2014.42 | 0.1000 | 2.50296 | 3.99 | 0.1200 |  |
| 36.6742 | 5012.58 | 0.1000 | 2.44845 | 9.93 | 0.1200 | 04-012-0632 |
| 36.7685 | 2506.29 | 0.1000 | 2.44845 | 4.97 | 0.1200 |  |
| 37.7226 | 546.30 | 0.1000 | 2.38277 | 1.08 | 0.1200 | 04-004-2852 |
| 37.8199 | 273.15 | 0.1000 | 2.38277 | 0.54 | 0.1200 |  |
| 38.7257 | 38871.82 | 0.1000 | 2.32333 | 77.03 | 0.1200 | 04-012-0632 |
| 38.8258 | 19435.91 | 0.1000 | 2.32333 | 38.52 | 0.1200 |  |
| 38.9268 | 50460.65 | 0.1000 | 2.31179 | 100.00 | 0.1200 | 04-012-0632 |
| 39.0274 | 25230.33 | 0.1000 | 2.31179 | 50.00 | 0.1200 |  |
| 39.2315 | 1016.10 | 0.1000 | 2.29454 | 2.01 | 0.1200 |  |
| 39.3329 | 508.05 | 0.1000 | 2.29454 | 1.01 | 0.1200 |  |
| 40.3931 | 838.37 | 0.1000 | 2.23119 | 1.66 | 0.1200 |  |
| 40.4978 | 419.19 | 0.1000 | 2.23119 | 0.83 | 0.1200 |  |
| 41.6684 | 24197.94 | 0.1000 | 2.16580 | 47.95 | 0.1200 | 04-012-0632, 04-004-2852 |
| 41.7767 | 12098.97 | 0.1000 | 2.16580 | 23.98 | 0.1200 |  |
| 43.2934 | 1324.65 | 0.1000 | 2.08820 | 2.63 | 0.1200 | 04-004-2852 |
| 43.4065 | 662.33 | 0.1000 | 2.08820 | 1.31 | 0.1200 |  |
| 44.8450 | 1650.22 | 0.1000 | 2.01949 | 3.27 | 0.1200 | 04-012-0632 |
| 44.9625 | 825.11 | 0.1000 | 2.01949 | 1.64 | 0.1200 |  |
| 48.3706 | 5942.37 | 0.1000 | 1.88020 | 11.78 | 0.1200 | 04-012-0632 |
| 48.4985 | 2971.19 | 0.1000 | 1.88020 | 5.89 | 0.1200 |  |
| 52.2200 | 2410.83 | 0.1000 | 1.75030 | 4.78 | 0.1200 | 04-012-0632 |
| 52.3596 | 1205.42 | 0.1000 | 1.75030 | 2.39 | 0.1200 |  |
| 52.4886 | 534.84 | 0.1000 | 1.74197 | 1.06 | 0.1200 | 04-004-2852 |
| 52.6291 | 267.42 | 0.1000 | 1.74197 | 0.53 | 0.1200 |  |
| 52.9351 | 188.99 | 0.1000 | 1.72833 | 0.37 | 0.1200 |  |
| 53.0769 | 94.49 | 0.1000 | 1.72833 | 0.19 | 0.1200 |  |
| 56.3535 | 8815.94 | 0.1000 | 1.63132 | 17.47 | 0.1200 | 04-012-0632 |
| 56.5061 | 4407.97 | 0.1000 | 1.63132 | 8.74 | 0.1200 |  |
| 57.4453 | 1456.93 | 0.1000 | 1.60289 | 2.89 | 0.1200 | 04-004-2852 |
| 57.6014 | 728.47 | 0.1000 | 1.60289 | 1.44 | 0.1200 |  |
| 60.1367 | 11746.68 | 0.1000 | 1.53742 | 23.28 | 0.1200 | 04-012-0632 |
| 60.3016 | 5873.34 | 0.1000 | 1.53742 | 11.64 | 0.1200 |  |
| 60.3966 | 2823.08 | 0.1000 | 1.53143 | 5.59 | 0.1200 |  |
| 60.5623 | 1411.54 | 0.1000 | 1.53143 | 2.80 | 0.1200 |  |
| 60.7646 | 3573.23 | 0.1000 | 1.52303 | 7.08 | 0.1200 | 04-012-0632 |
| 60.9316 | 1786.62 | 0.1000 | 1.52303 | 3.54 | 0.1200 |  |
| 63.7176 | 321.49 | 0.1000 | 1.45938 | 0.64 | 0.1200 | 04-012-0632 |
| 63.8946 | 160.74 | 0.1000 | 1.45938 | 0.32 | 0.1200 |  |
| 65.4062 | 3337.34 | 0.1000 | 1.42572 | 6.61 | 0.1200 | 04-012-0632 |
| 65.5891 | 1668.67 | 0.1000 | 1.42572 | 3.31 | 0.1200 |  |
| 66.4694 | 428.24 | 0.1000 | 1.40548 | 0.85 | 0.1200 | 04-004-2852 |
| 66.6561 | 214.12 | 0.1000 | 1.40548 | 0.42 | 0.1200 |  |
| 68.1590 | 694.56 | 0.1000 | 1.37469 | 1.38 | 0.1200 | 04-004-2852 |
| 68.3517 | 347.28 | 0.1000 | 1.37469 | 0.69 | 0.1200 |  |

# Identified Patterns List: (Bookmark4)

| Visible | Ref.Code | Score | Compound Name | Displ.[°2θ] | Scale Fac. | Chem. Formula |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-012-0632 | 39 | Titanium Aluminum Carbide | -0.158 | 0.395 | Ti3 Al C2 |
| * | 04-004-2852 | 53 | Aluminum Oxide | -0.099 | 0.023 | Al2 O3 |

# Plot of Identified Phases: (Bookmark 5)

# Document History: (Bookmark 6)

Beam attenuation factor(s) used to back-calculate ESDs:

- Modification time = "19/09/2019 09:31:41"

- Modification editor = "xrdpc2"

Insert Measurement:

- File name = "Ti3AlC2_30-08_20190918.xrdml"

- Modification time = "19/09/2019 09:31:41"

- Modification editor = "xrdpc2"

Default properties:

- Measurement step axis = "None"

- Internal wavelengths used from anode material: Copper (Cu)

- Original K-Alpha1 wavelength = "1.54060"

- Used K-Alpha1 wavelength = "1.54060"

- Original K-Alpha2 wavelength = "1.54443"

- Used K-Alpha2 wavelength = "1.54443"

- Original K-Beta wavelength = "1.39225"

- Used K-Beta wavelength = "1.39225"

- Irradiated length = "10.00000"

- Receiving slit size = "0.10000"

- Step axis value = "0.00000"

- Offset = "0.00000"

- Sample length = "10.00000"

- Modification time = "19/09/2019 09:31:41"

- Modification editor = "xrdpc2"

Interpolate Step Size:

- Initial Scan Range = 5.00136 - 69.99150

- Initial Step Size = 0.01671

- Derived Step Size = 0.01700

- Use Derived Step Size = "Yes"

- Modification time = "19/09/2019 09:31:41"

- Modification editor = "PANalytical"

Take As Anchor Scan:

- Scan name = "Ti3AlC2_30-08_20190918"

- Modification time = "19/09/2019 09:40:53"

- Modification editor = "xrdpc2"

Take As Anchor Scan:

- Scan name = "Ti3AlC2_30-08_20190918"

- Modification time = "19/09/2019 09:40:56"

- Modification editor = "xrdpc2"

Take As Anchor Scan:

- Scan name = "Ti3AlC2_30-08_20190918"

- Modification time = "19/09/2019 09:41:24"

- Modification editor = "xrdpc2"

Take As Anchor Scan:

- Scan name = "Ti3AlC2_30-08_20190918"

- Modification time = "19/09/2019 09:56:38"

- Modification editor = "xrdpc2"

Determine Background:

- Add to net scan = "Nothing"

- User defined intensity = "-5"

- Correction method = "Automatic"

- Bending factor = "5"

- Minimum significance = "0.7"

- Minimum tip width = "0"

- Maximum tip width = "1"

- Peak base width = "2"

- Use smoothed input data = "Yes"

- Granularity = "20"

- Modification time = "22/02/2001 10:17:43"

- Modification editor = "PANalytical"

Take As Anchor Scan:

- Scan name = "Ti3AlC2_30-08_20190918"

- Modification time = "19/09/2019 09:57:43"

- Modification editor = "xrdpc2"

Take As Anchor Scan:

- Scan name = "Ti3AlC2_30-08_20190918"

- Modification time = "19/09/2019 10:31:40"

- Modification editor = "xrdpc2"

Take As Anchor Scan:

- Scan name = "Ti3AlC2_30-08_20190918"

- Modification time = "19/09/2019 10:31:45"

- Modification editor = "xrdpc2"

Search Peaks:

- Minimum significance = "2"

- Minimum tip width = "0.01"

- Maximum tip width = "1"

- Peak base width = "2"

- Method = "Minimum 2nd derivative"

- Modification time = "20/02/2001 11:55:18"

- Modification editor = "PANalytical"

Profile/Rietveld fitting:

- Angular range Gonio = "5.001 - 10.900"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "8"

- Chi Square = "23.5656149513495"

- Rp = "0.13530"

- Rwp = "0.20667"

- Rexp = "0.00877"

- BCLM Exit Code = "Refinement iterations exceeded"

- Modification time = "19/09/2019 10:32:46"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "5.001 - 8.129"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "4"

- Chi Square = "31.936213085079"

- Rp = "0.18278"

- Rwp = "0.24752"

- Rexp = "0.00775"

- Modification time = "19/09/2019 10:32:58"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "10.914 - 22.389"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "20"

- Chi Square = "2.00808125838661"

- Rp = "0.02019"

- Rwp = "0.03171"

- Rexp = "0.01579"

- Modification time = "19/09/2019 10:33:15"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "21.423 - 32.898"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "8"

- Chi Square = "3.0561528765184"

- Rp = "0.03693"

- Rwp = "0.06648"

- Rexp = "0.02175"

- Modification time = "19/09/2019 10:34:10"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "31.382 - 37.468"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "20"

- Chi Square = "2.18998816503052"

- Rp = "0.03036"

- Rwp = "0.04099"

- Rexp = "0.01872"

- Modification time = "19/09/2019 10:34:25"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "37.366 - 40.885"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "20"

- Chi Square = "5.52608070942945"

- Rp = "0.04288"

- Rwp = "0.05971"

- Rexp = "0.01081"

- Modification time = "19/09/2019 10:34:38"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "40.956 - 44.475"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "8"

- Chi Square = "3.76063431163247"

- Rp = "0.04427"

- Rwp = "0.05830"

- Rexp = "0.01550"

- Modification time = "19/09/2019 10:34:47"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "43.965 - 47.484"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "4"

- Chi Square = "1.08648974480824"

- Rp = "0.02110"

- Rwp = "0.02672"

- Rexp = "0.02459"

- Modification time = "19/09/2019 10:34:56"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "46.804 - 50.323"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "4"

- Chi Square = "2.05212836981386"

- Rp = "0.04322"

- Rwp = "0.05370"

- Rexp = "0.02617"

- Modification time = "19/09/2019 10:35:04"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "51.394 - 54.913"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "12"

- Chi Square = "1.60461863570662"

- Rp = "0.03454"

- Rwp = "0.04592"

- Rexp = "0.02862"

- Modification time = "19/09/2019 10:35:11"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "55.304 - 58.823"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "8"

- Chi Square = "3.98064469574253"

- Rp = "0.07474"

- Rwp = "0.09250"

- Rexp = "0.02324"

- Modification time = "19/09/2019 10:35:18"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "59.367 - 62.886"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "12"

- Chi Square = "5.65591093685208"

- Rp = "0.07577"

- Rwp = "0.10837"

- Rexp = "0.01916"

- Modification time = "19/09/2019 10:35:27"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "63.447 - 66.966"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "12"

- Chi Square = "2.10277342283451"

- Rp = "0.04292"

- Rwp = "0.05605"

- Rexp = "0.02666"

- Modification time = "19/09/2019 10:35:44"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "67.405 - 69.377"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "4"

- Chi Square = "2.43565813874869"

- Rp = "0.04537"

- Rwp = "0.07542"

- Rexp = "0.03097"

- Modification time = "19/09/2019 10:35:57"

- Modification editor = "xrdpc2"

Search & Match:

- Allow pattern shift = "Yes"

- Auto residue = "Yes"

- Data source = "Profile and peak list"

- Demote unmatched strong = "No"

- Multi phase = "Yes"

- Restriction set = "Untitled"

- Restriction = "Restriction set"

- Subset name = ""

- Match intensity = "No"

- Two theta shift = "-0.3"

- Identify = "No"

- Max. no. of accepted patterns = "5"

- Minimum score = "50"

- Min. new lines / total lines = "60"

- Search depth = "10"

- Minimum new lines = "5"

- Minimum scale factor = "0.1"

- Intensity threshold = "0"

- Use line clustering = "Yes"

- Line cluster range = "1.5"

- Search sensitivity = "1.8"

- Use adaptive smoothing = "Yes"

- Smoothing range = "1.5"

- Threshold factor = "3"

- Match Threshold = "0"

- N * Esds = "-1"

- Raw Weight = "-1"

- Peak Shape = "-1"

- Accepted Shape = "-1"

- Peak Power = "-1"

- New Peak Power = "-1"

- Intensity Power = "-1"

- N Peaks Power = "-1"

- Modification time = "19/09/2019 10:20:20"

- Modification editor = "xrdpc2"

Delete Peak(s):

- Start position = "17.9470"

- End position = "17.9920"

- Modification time = "19/09/2019 10:38:57"

- Modification editor = "xrdpc2"

Delete Peak(s):

- Start position = "21.0738"

- End position = "21.1267"

- Modification time = "19/09/2019 10:39:17"

- Modification editor = "xrdpc2"