Fantastic report on

input.doc

Distribution:

| Name | Function | 0.1 | 0.5 | 1.0 |
| --- | --- | --- | --- | --- |
| N.N.-999 | Masterking Group Manager (MGM) |  |  |  |
| N.N.-998 | Product Ontwikkelt Manager (POM) |  |  |  |
| N.N.-1 | (AS) |  |  |  |
| N.N.-2 | (DS) |  |  |  |
| N.N.-3 | (BS) |  |  |  |
| T.P. | Supervisor All Coding |  |  |  |

# Table of Contents:

Table of Contents:	2

Anchor Scan Parameters: (Bookmark1)	3

Graphics: (Bookmark2)	4

Peak List: (Bookmark 3)	5

Identified Patterns List: (Bookmark4)	7

Plot of Identified Phases: (Bookmark 5)	7

Document History: (Bookmark 6)	8

# Anchor Scan Parameters: (Bookmark1)

Dataset Name	Ti3AlC2_03-07_20190918

File name	Y:\James Bird\Training\Ti3AlC2 or Ti3C2Tx\Ti3AlC2_03-07_20190918.xrdml

Sample Identification	03-07

Comment	Configuration=Spinner, Owner=User-1, Creation date=08/12/2015 14:27:11

Goniometer=PW3050/60 (Theta/Theta); Minimum step size 2Theta:0.001; Minimum step size Omega:0.001

Sample stage=Spinner PW3064

Diffractometer system=XPERT-PRO

Measurement program=James Bird 10mm Mask Refinement, Owner=User-1, Creation date=18/09/2019 16:54:35

Refinement

Measurement Start Date/Time	18/09/2019 17:02:26

Operator	xrduser

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	5.0014

End Position [°2θ]	69.9754

Step Size [°2θ]	0.0170

Scan Step Time [s]	514.9850

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	2.12

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.2500

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-Alpha1 [Å]	1.54060

K-Alpha2 [Å]	1.54443

K-Beta [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	40 mA, 40 kV

Diffractometer Type	0000000000007141

Diffractometer Number	0

Goniometer Radius [mm]	240.00

Dist. Focus-Diverg. Slit [mm]	100.00

Incident Beam Monochromator	No

Spinning	Yes

# Graphics: (Bookmark2)

# Peak List: (Bookmark 3)

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] | Tip Width | Matched by |
| --- | --- | --- | --- | --- | --- | --- |
| 6.3930 | 2770.62 | 0.1000 | 13.81447 | 10.74 | 0.1200 |  |
| 6.4089 | 1385.31 | 0.1000 | 13.81447 | 5.37 | 0.1200 |  |
| 9.5347 | 6386.94 | 0.1000 | 9.26848 | 24.77 | 0.1200 | 04-012-0632 |
| 9.5584 | 3193.47 | 0.1000 | 9.26848 | 12.38 | 0.1200 |  |
| 19.1216 | 2090.58 | 0.1000 | 4.63772 | 8.11 | 0.1200 | 04-012-0632 |
| 19.1696 | 1045.29 | 0.1000 | 4.63772 | 4.05 | 0.1200 |  |
| 25.5899 | 385.02 | 0.1000 | 3.47823 | 1.49 | 0.1200 | 04-004-2852 |
| 25.6546 | 192.51 | 0.1000 | 3.47823 | 0.75 | 0.1200 |  |
| 27.1121 | 2176.96 | 0.1000 | 3.28631 | 8.44 | 0.1200 | 04-003-0648 |
| 27.1807 | 1088.48 | 0.1000 | 3.28631 | 4.22 | 0.1200 |  |
| 28.8415 | 256.26 | 0.1000 | 3.09307 | 0.99 | 0.1200 | 04-012-0632 |
| 28.9147 | 128.13 | 0.1000 | 3.09307 | 0.50 | 0.1200 |  |
| 34.0138 | 5375.80 | 0.1000 | 2.63362 | 20.85 | 0.1200 | 04-012-0632 |
| 34.1009 | 2687.90 | 0.1000 | 2.63362 | 10.42 | 0.1200 |  |
| 35.1346 | 1484.28 | 0.1000 | 2.55213 | 5.76 | 0.1200 | 04-004-2852 |
| 35.2248 | 742.14 | 0.1000 | 2.55213 | 2.88 | 0.1200 |  |
| 35.9235 | 3636.99 | 0.1000 | 2.49787 | 14.10 | 0.1200 |  |
| 36.0158 | 1818.50 | 0.1000 | 2.49787 | 7.05 | 0.1200 |  |
| 36.7416 | 2305.61 | 0.1000 | 2.44411 | 8.94 | 0.1200 | 04-012-0632 |
| 36.8362 | 1152.80 | 0.1000 | 2.44411 | 4.47 | 0.1200 |  |
| 37.7985 | 309.02 | 0.1000 | 2.37816 | 1.20 | 0.1200 | 04-004-2852 |
| 37.8960 | 154.51 | 0.1000 | 2.37816 | 0.60 | 0.1200 |  |
| 38.7883 | 24493.05 | 0.1000 | 2.31972 | 94.98 | 0.1200 | 04-012-0632, 04-003-0648 |
| 38.8886 | 12246.52 | 0.1000 | 2.31972 | 47.49 | 0.1200 |  |
| 38.9939 | 25787.93 | 0.1000 | 2.30797 | 100.00 | 0.1200 | 04-012-0632 |
| 39.0947 | 12893.97 | 0.1000 | 2.30797 | 50.00 | 0.1200 |  |
| 40.4481 | 318.16 | 0.1000 | 2.22828 | 1.23 | 0.1200 |  |
| 40.5530 | 159.08 | 0.1000 | 2.22828 | 0.62 | 0.1200 |  |
| 41.0573 | 609.13 | 0.1000 | 2.19661 | 2.36 | 0.1200 |  |
| 41.1640 | 304.57 | 0.1000 | 2.19661 | 1.18 | 0.1200 |  |
| 41.7283 | 12840.13 | 0.1000 | 2.16283 | 49.79 | 0.1200 | 04-012-0632, 04-004-2852 |
| 41.8369 | 6420.06 | 0.1000 | 2.16283 | 24.90 | 0.1200 |  |
| 43.3670 | 957.56 | 0.1000 | 2.08483 | 3.71 | 0.1200 | 04-004-2852 |
| 43.4802 | 478.78 | 0.1000 | 2.08483 | 1.86 | 0.1200 |  |
| 44.9084 | 794.85 | 0.1000 | 2.01678 | 3.08 | 0.1200 | 04-012-0632 |
| 45.0261 | 397.42 | 0.1000 | 2.01678 | 1.54 | 0.1200 |  |
| 48.4391 | 3038.07 | 0.1000 | 1.87771 | 11.78 | 0.1200 | 04-012-0632 |
| 48.5672 | 1519.03 | 0.1000 | 1.87771 | 5.89 | 0.1200 |  |
| 52.2907 | 1217.48 | 0.1000 | 1.74810 | 4.72 | 0.1200 | 04-012-0632 |
| 52.4305 | 608.74 | 0.1000 | 1.74810 | 2.36 | 0.1200 |  |
| 53.9585 | 1510.70 | 0.1000 | 1.69794 | 5.86 | 0.1200 | 04-003-0648 |
| 54.1035 | 755.35 | 0.1000 | 1.69794 | 2.93 | 0.1200 |  |
| 56.4158 | 4830.94 | 0.1000 | 1.62967 | 18.73 | 0.1200 | 04-012-0632, 04-003-0648 |
| 56.5686 | 2415.47 | 0.1000 | 1.62967 | 9.37 | 0.1200 |  |
| 57.5076 | 1051.17 | 0.1000 | 1.60130 | 4.08 | 0.1200 | 04-004-2852 |
| 57.6639 | 525.59 | 0.1000 | 1.60130 | 2.04 | 0.1200 |  |
| 60.2167 | 6602.56 | 0.1000 | 1.53557 | 25.60 | 0.1200 | 04-012-0632 |
| 60.3819 | 3301.28 | 0.1000 | 1.53557 | 12.80 | 0.1200 |  |
| 60.9133 | 2109.84 | 0.1000 | 1.51967 | 8.18 | 0.1200 |  |
| 61.0808 | 1054.92 | 0.1000 | 1.51967 | 4.09 | 0.1200 |  |
| 62.9264 | 299.99 | 0.1000 | 1.47581 | 1.16 | 0.1200 |  |
| 63.1007 | 149.99 | 0.1000 | 1.47581 | 0.58 | 0.1200 |  |
| 65.4712 | 2094.10 | 0.1000 | 1.42447 | 8.12 | 0.1200 | 04-012-0632 |
| 65.6544 | 1047.05 | 0.1000 | 1.42447 | 4.06 | 0.1200 |  |
| 66.5296 | 272.38 | 0.1000 | 1.40435 | 1.06 | 0.1200 | 04-004-2852 |
| 66.7165 | 136.19 | 0.1000 | 1.40435 | 0.53 | 0.1200 |  |
| 68.2315 | 646.19 | 0.1000 | 1.37341 | 2.51 | 0.1200 | 04-004-2852 |
| 68.4245 | 323.10 | 0.1000 | 1.37341 | 1.25 | 0.1200 |  |

# Identified Patterns List: (Bookmark4)

| Visible | Ref.Code | Score | Compound Name | Displ.[°2θ] | Scale Fac. | Chem. Formula |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-012-0632 | 51 | Titanium Aluminum Carbide | -0.069 | 0.677 | Ti3 Al C2 |
| * | 04-004-2852 | 56 | Aluminum Oxide | -0.033 | 0.034 | Al2 O3 |
| * | 04-003-0648 | 38 | Titanium Oxide | -0.312 | 0.079 | Ti O2 |

# Plot of Identified Phases: (Bookmark 5)

# Document History: (Bookmark 6)

Beam attenuation factor(s) used to back-calculate ESDs:

- Modification time = "19/09/2019 09:31:41"

- Modification editor = "xrdpc2"

Insert Measurement:

- File name = "Ti3AlC2_03-07_20190918.xrdml"

- Modification time = "19/09/2019 09:31:41"

- Modification editor = "xrdpc2"

Default properties:

- Measurement step axis = "None"

- Internal wavelengths used from anode material: Copper (Cu)

- Original K-Alpha1 wavelength = "1.54060"

- Used K-Alpha1 wavelength = "1.54060"

- Original K-Alpha2 wavelength = "1.54443"

- Used K-Alpha2 wavelength = "1.54443"

- Original K-Beta wavelength = "1.39225"

- Used K-Beta wavelength = "1.39225"

- Irradiated length = "10.00000"

- Receiving slit size = "0.10000"

- Step axis value = "0.00000"

- Offset = "0.00000"

- Sample length = "10.00000"

- Modification time = "19/09/2019 09:31:41"

- Modification editor = "xrdpc2"

Interpolate Step Size:

- Initial Scan Range = 5.00136 - 69.99150

- Initial Step Size = 0.01671

- Derived Step Size = 0.01700

- Use Derived Step Size = "Yes"

- Modification time = "19/09/2019 09:31:41"

- Modification editor = "PANalytical"

Take As Anchor Scan:

- Scan name = "Ti3AlC2_03-07_20190918"

- Modification time = "19/09/2019 09:40:55"

- Modification editor = "xrdpc2"

Take As Anchor Scan:

- Scan name = "Ti3AlC2_03-07_20190918"

- Modification time = "19/09/2019 09:40:59"

- Modification editor = "xrdpc2"

Take As Anchor Scan:

- Scan name = "Ti3AlC2_03-07_20190918"

- Modification time = "19/09/2019 09:53:04"

- Modification editor = "xrdpc2"

Determine Background:

- Add to net scan = "Nothing"

- User defined intensity = "-5"

- Correction method = "Automatic"

- Bending factor = "5"

- Minimum significance = "0.7"

- Minimum tip width = "0"

- Maximum tip width = "1"

- Peak base width = "2"

- Use smoothed input data = "Yes"

- Granularity = "20"

- Modification time = "22/02/2001 10:17:43"

- Modification editor = "PANalytical"

Take As Anchor Scan:

- Scan name = "Ti3AlC2_03-07_20190918"

- Modification time = "19/09/2019 09:57:00"

- Modification editor = "xrdpc2"

Take As Anchor Scan:

- Scan name = "Ti3AlC2_03-07_20190918"

- Modification time = "19/09/2019 09:57:44"

- Modification editor = "xrdpc2"

Take As Anchor Scan:

- Scan name = "Ti3AlC2_03-07_20190918"

- Modification time = "19/09/2019 09:58:54"

- Modification editor = "xrdpc2"

Search Peaks:

- Minimum significance = "2"

- Minimum tip width = "0.01"

- Maximum tip width = "1"

- Peak base width = "2"

- Method = "Minimum 2nd derivative"

- Modification time = "20/02/2001 11:55:18"

- Modification editor = "PANalytical"

Profile/Rietveld fitting:

- Angular range Gonio = "5.100 - 7.820"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "4"

- Chi Square = "6.03818576557072"

- Rp = "0.04542"

- Rwp = "0.06176"

- Rexp = "0.01023"

- Modification time = "19/09/2019 10:02:04"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "5.001 - 8.962"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "4"

- Chi Square = "4.97584610802179"

- Rp = "0.03658"

- Rwp = "0.05404"

- Rexp = "0.01086"

- Modification time = "19/09/2019 10:02:14"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "5.001 - 8.962"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "4"

- Chi Square = "4.97015071248719"

- Rp = "0.03655"

- Rwp = "0.05398"

- Rexp = "0.01086"

- Modification time = "19/09/2019 10:02:21"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "5.001 - 8.129"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "4"

- Chi Square = "5.58612226443159"

- Rp = "0.04136"

- Rwp = "0.05808"

- Rexp = "0.01040"

- Modification time = "19/09/2019 10:02:48"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "8.466 - 10.557"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "4"

- Chi Square = "4.79437131014514"

- Rp = "0.04089"

- Rwp = "0.06094"

- Rexp = "0.01271"

- Modification time = "19/09/2019 10:03:26"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "17.680 - 19.992"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "4"

- Chi Square = "1.12274211048303"

- Rp = "0.01676"

- Rwp = "0.02047"

- Rexp = "0.01823"

- Modification time = "19/09/2019 10:03:46"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "26.112 - 28.288"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "4"

- Chi Square = "6.90694752854994"

- Rp = "0.11509"

- Rwp = "0.13786"

- Rexp = "0.01996"

- Modification time = "19/09/2019 10:06:12"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "22.712 - 31.943"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "12"

- Chi Square = "3.44745413498036"

- Rp = "0.04646"

- Rwp = "0.07751"

- Rexp = "0.02248"

- Modification time = "19/09/2019 10:06:24"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "23.817 - 30.702"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "12"

- Chi Square = "3.95755623210326"

- Rp = "0.05404"

- Rwp = "0.08668"

- Rexp = "0.02190"

- Modification time = "19/09/2019 10:06:34"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "30.535 - 37.420"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "16"

- Chi Square = "1.66331304154357"

- Rp = "0.02924"

- Rwp = "0.03671"

- Rexp = "0.02207"

- Modification time = "19/09/2019 10:06:54"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "37.485 - 39.950"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "12"

- Chi Square = "7.8966137931425"

- Rp = "0.07420"

- Rwp = "0.09365"

- Rexp = "0.01186"

- Modification time = "19/09/2019 10:07:58"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "39.712 - 42.092"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "12"

- Chi Square = "4.59927207930908"

- Rp = "0.05717"

- Rwp = "0.07542"

- Rexp = "0.01640"

- Modification time = "19/09/2019 10:08:21"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "43.064 - 45.444"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "8"

- Chi Square = "1.33404105842273"

- Rp = "0.02416"

- Rwp = "0.03125"

- Rexp = "0.02342"

- Modification time = "19/09/2019 10:08:34"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "47.484 - 49.864"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "4"

- Chi Square = "1.94616432224721"

- Rp = "0.04269"

- Rwp = "0.05394"

- Rexp = "0.02772"

- Modification time = "19/09/2019 10:08:48"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "50.915 - 58.769"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "16"

- Chi Square = "3.19736737839766"

- Rp = "0.06585"

- Rwp = "0.08546"

- Rexp = "0.02673"

- Modification time = "19/09/2019 10:09:07"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "59.211 - 62.118"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "8"

- Chi Square = "8.66390027969794"

- Rp = "0.14567"

- Rwp = "0.18928"

- Rexp = "0.02185"

- Modification time = "19/09/2019 10:09:31"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "58.565 - 69.972"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "24"

- Chi Square = "4.84926530279581"

- Rp = "0.08984"

- Rwp = "0.13158"

- Rexp = "0.02713"

- Modification time = "19/09/2019 10:09:48"

- Modification editor = "xrdpc2"

Search & Match:

- Allow pattern shift = "Yes"

- Auto residue = "Yes"

- Data source = "Profile and peak list"

- Demote unmatched strong = "No"

- Multi phase = "Yes"

- Restriction set = "Untitled"

- Restriction = "Restriction set"

- Subset name = ""

- Match intensity = "No"

- Two theta shift = "-0.3"

- Identify = "No"

- Max. no. of accepted patterns = "5"

- Minimum score = "50"

- Min. new lines / total lines = "60"

- Search depth = "10"

- Minimum new lines = "5"

- Minimum scale factor = "0.1"

- Intensity threshold = "0"

- Use line clustering = "Yes"

- Line cluster range = "1.5"

- Search sensitivity = "1.8"

- Use adaptive smoothing = "Yes"

- Smoothing range = "1.5"

- Threshold factor = "3"

- Match Threshold = "0"

- N * Esds = "-1"

- Raw Weight = "-1"

- Peak Shape = "-1"

- Accepted Shape = "-1"

- Peak Power = "-1"

- New Peak Power = "-1"

- Intensity Power = "-1"

- N Peaks Power = "-1"

- Modification time = "19/09/2019 10:19:25"

- Modification editor = "xrdpc2"