Fantastic report on

input.doc

Distribution:

| Name | Function | 0.1 | 0.5 | 1.0 |
| --- | --- | --- | --- | --- |
| N.N.-999 | Masterking Group Manager (MGM) |  |  |  |
| N.N.-998 | Product Ontwikkelt Manager (POM) |  |  |  |
| N.N.-1 | (AS) |  |  |  |
| N.N.-2 | (DS) |  |  |  |
| N.N.-3 | (BS) |  |  |  |
| T.P. | Supervisor All Coding |  |  |  |

# Table of Contents:

Table of Contents:	2

Anchor Scan Parameters: (Bookmark1)	3

Graphics: (Bookmark2)	4

Peak List: (Bookmark 3)	5

Identified Patterns List: (Bookmark4)	7

Plot of Identified Phases: (Bookmark 5)	7

Document History: (Bookmark 6)	8

# Anchor Scan Parameters: (Bookmark1)

Dataset Name	Ti3C2_20190918

File name	Y:\James Bird\Training\Ti3AlC2 or Ti3C2Tx\Ti3C2_20190918.xrdml

Comment	Configuration=Spinner, Owner=User-1, Creation date=08/12/2015 14:27:11

Goniometer=PW3050/60 (Theta/Theta); Minimum step size 2Theta:0.001; Minimum step size Omega:0.001

Sample stage=Spinner PW3064

Diffractometer system=XPERT-PRO

Measurement program=James Bird 10mm Mask, Owner=User-1, Creation date=22/07/2019 14:48:21

1h 5-70

Measurement Start Date/Time	19/09/2019 02:07:27

Operator	xrduser

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	5.0097

End Position [°2θ]	69.9537

Step Size [°2θ]	0.0330

Scan Step Time [s]	219.7100

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	2.12

Offset [°2θ]	0.0000

Divergence Slit Type	Automatic

Irradiated Length [mm]	8.00

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-Alpha1 [Å]	1.54060

K-Alpha2 [Å]	1.54443

K-Beta [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	40 mA, 40 kV

Diffractometer Type	0000000000007141

Diffractometer Number	0

Goniometer Radius [mm]	240.00

Dist. Focus-Diverg. Slit [mm]	100.00

Incident Beam Monochromator	No

Spinning	Yes

# Graphics: (Bookmark2)

# Peak List: (Bookmark 3)

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] | Tip Width | Matched by |
| --- | --- | --- | --- | --- | --- | --- |
| 5.4845 | 1073.80 | 0.1000 | 16.10045 | 3.08 | 0.1200 |  |
| 5.4982 | 536.90 | 0.1000 | 16.10045 | 1.54 | 0.1200 |  |
| 5.7284 | 1515.24 | 0.1000 | 15.41568 | 4.34 | 0.1200 |  |
| 5.7426 | 757.62 | 0.1000 | 15.41568 | 2.17 | 0.1200 |  |
| 5.9926 | 2265.25 | 0.1000 | 14.73654 | 6.49 | 0.1200 |  |
| 6.0075 | 1132.63 | 0.1000 | 14.73654 | 3.25 | 0.1200 |  |
| 6.2921 | 2923.13 | 0.1000 | 14.03580 | 8.38 | 0.1200 |  |
| 6.3077 | 1461.56 | 0.1000 | 14.03580 | 4.19 | 0.1200 |  |
| 6.6735 | 1822.34 | 0.1000 | 13.23442 | 5.22 | 0.1200 |  |
| 6.6901 | 911.17 | 0.1000 | 13.23442 | 2.61 | 0.1200 |  |
| 7.0909 | 548.20 | 0.1000 | 12.45629 | 1.57 | 0.1200 |  |
| 7.1085 | 274.10 | 0.1000 | 12.45629 | 0.79 | 0.1200 |  |
| 9.6171 | 3439.00 | 0.1000 | 9.18915 | 9.86 | 0.1200 |  |
| 9.6411 | 1719.50 | 0.1000 | 9.18915 | 4.93 | 0.1200 |  |
| 18.0934 | 172.27 | 0.1000 | 4.89889 | 0.49 | 0.1200 |  |
| 18.1387 | 86.13 | 0.1000 | 4.89889 | 0.25 | 0.1200 |  |
| 19.2011 | 1946.34 | 0.1000 | 4.61870 | 5.58 | 0.1200 |  |
| 19.2493 | 973.17 | 0.1000 | 4.61870 | 2.79 | 0.1200 |  |
| 25.5829 | 605.43 | 0.1000 | 3.47917 | 1.74 | 0.1200 |  |
| 25.6475 | 302.71 | 0.1000 | 3.47917 | 0.87 | 0.1200 |  |
| 27.1707 | 8236.01 | 0.1000 | 3.27936 | 23.60 | 0.1200 | 04-003-0648 |
| 27.2395 | 4118.01 | 0.1000 | 3.27936 | 11.80 | 0.1200 |  |
| 28.9263 | 397.51 | 0.1000 | 3.08419 | 1.14 | 0.1200 |  |
| 28.9997 | 198.76 | 0.1000 | 3.08419 | 0.57 | 0.1200 |  |
| 34.0913 | 2217.66 | 0.1000 | 2.62781 | 6.36 | 0.1200 |  |
| 34.1787 | 1108.83 | 0.1000 | 2.62781 | 3.18 | 0.1200 |  |
| 35.2233 | 1099.74 | 0.1000 | 2.54591 | 3.15 | 0.1200 |  |
| 35.3137 | 549.87 | 0.1000 | 2.54591 | 1.58 | 0.1200 |  |
| 36.0286 | 4515.49 | 0.1000 | 2.49083 | 12.94 | 0.1200 |  |
| 36.1212 | 2257.74 | 0.1000 | 2.49083 | 6.47 | 0.1200 |  |
| 36.8308 | 1017.35 | 0.1000 | 2.43840 | 2.92 | 0.1200 |  |
| 36.9256 | 508.68 | 0.1000 | 2.43840 | 1.46 | 0.1200 |  |
| 37.8671 | 345.17 | 0.1000 | 2.37401 | 0.99 | 0.1200 |  |
| 37.9648 | 172.59 | 0.1000 | 2.37401 | 0.49 | 0.1200 |  |
| 38.8758 | 34892.94 | 0.1000 | 2.31471 | 100.00 | 0.1200 | 04-003-0648 |
| 38.9763 | 17446.47 | 0.1000 | 2.31471 | 50.00 | 0.1200 |  |
| 39.0757 | 12021.33 | 0.1000 | 2.30332 | 34.45 | 0.1200 |  |
| 39.1768 | 6010.67 | 0.1000 | 2.30332 | 17.23 | 0.1200 |  |
| 40.9945 | 1307.45 | 0.1000 | 2.19983 | 3.75 | 0.1200 | 04-003-0648 |
| 41.1010 | 653.72 | 0.1000 | 2.19983 | 1.87 | 0.1200 |  |
| 41.1875 | 2746.32 | 0.1000 | 2.18997 | 7.87 | 0.1200 |  |
| 41.2945 | 1373.16 | 0.1000 | 2.18997 | 3.94 | 0.1200 |  |
| 41.8158 | 8618.54 | 0.1000 | 2.15851 | 24.70 | 0.1200 |  |
| 41.9246 | 4309.27 | 0.1000 | 2.15851 | 12.35 | 0.1200 |  |
| 43.4724 | 2235.98 | 0.1000 | 2.08001 | 6.41 | 0.1200 |  |
| 43.5860 | 1117.99 | 0.1000 | 2.08001 | 3.20 | 0.1200 |  |
| 45.0220 | 487.52 | 0.1000 | 2.01195 | 1.40 | 0.1200 |  |
| 45.1401 | 243.76 | 0.1000 | 2.01195 | 0.70 | 0.1200 |  |
| 48.5188 | 2021.30 | 0.1000 | 1.87481 | 5.79 | 0.1200 |  |
| 48.6472 | 1010.65 | 0.1000 | 1.87481 | 2.90 | 0.1200 |  |
| 52.3610 | 963.96 | 0.1000 | 1.74591 | 2.76 | 0.1200 | 00-046-1212 |
| 52.5011 | 481.98 | 0.1000 | 1.74591 | 1.38 | 0.1200 |  |
| 53.9894 | 8313.18 | 0.1000 | 1.69704 | 23.82 | 0.1200 | 04-003-0648 |
| 54.1345 | 4156.59 | 0.1000 | 1.69704 | 11.91 | 0.1200 |  |
| 56.0052 | 2950.85 | 0.1000 | 1.64064 | 8.46 | 0.1200 | 04-012-0632 |
| 56.1567 | 1475.43 | 0.1000 | 1.64064 | 4.23 | 0.1200 |  |
| 56.4839 | 4109.01 | 0.1000 | 1.62786 | 11.78 | 0.1200 |  |
| 56.6369 | 2054.50 | 0.1000 | 1.62786 | 5.89 | 0.1200 |  |
| 57.5779 | 1246.25 | 0.1000 | 1.59951 | 3.57 | 0.1200 |  |
| 57.7344 | 623.13 | 0.1000 | 1.59951 | 1.79 | 0.1200 |  |
| 60.2730 | 3528.77 | 0.1000 | 1.53427 | 10.11 | 0.1200 |  |
| 60.4384 | 1764.39 | 0.1000 | 1.53427 | 5.06 | 0.1200 |  |
| 60.5271 | 2586.15 | 0.1000 | 1.52844 | 7.41 | 0.1200 | 04-012-0632 |
| 60.6933 | 1293.07 | 0.1000 | 1.52844 | 3.71 | 0.1200 |  |
| 60.8862 | 1172.64 | 0.1000 | 1.52028 | 3.36 | 0.1200 | 04-012-0632, 00-046-1212 |
| 61.0186 | 1306.88 | 0.1000 | 1.51730 | 3.75 | 0.1200 | 00-046-1212 |
| 61.0536 | 586.32 | 0.1000 | 1.52028 | 1.68 | 0.1200 |  |
| 61.1864 | 653.44 | 0.1000 | 1.51730 | 1.87 | 0.1200 |  |
| 61.3513 | 610.63 | 0.1000 | 1.50987 | 1.75 | 0.1200 |  |
| 61.5202 | 305.32 | 0.1000 | 1.50987 | 0.88 | 0.1200 |  |
| 63.0681 | 1566.83 | 0.1000 | 1.47283 | 4.49 | 0.1200 |  |
| 63.2429 | 783.42 | 0.1000 | 1.47283 | 2.25 | 0.1200 |  |
| 63.4317 | 1043.01 | 0.1000 | 1.46526 | 2.99 | 0.1200 | 04-012-0632 |
| 63.6077 | 521.50 | 0.1000 | 1.46526 | 1.49 | 0.1200 |  |
| 65.5303 | 1657.78 | 0.1000 | 1.42333 | 4.75 | 0.1200 |  |
| 65.7136 | 828.89 | 0.1000 | 1.42333 | 2.38 | 0.1200 |  |
| 66.6028 | 339.53 | 0.1000 | 1.40298 | 0.97 | 0.1200 |  |
| 66.7900 | 169.77 | 0.1000 | 1.40298 | 0.49 | 0.1200 |  |
| 68.2785 | 1982.87 | 0.1000 | 1.37258 | 5.68 | 0.1200 |  |
| 68.4717 | 991.43 | 0.1000 | 1.37258 | 2.84 | 0.1200 |  |
| 68.5170 | 1597.95 | 0.1000 | 1.36838 | 4.58 | 0.1200 |  |
| 68.7111 | 798.98 | 0.1000 | 1.36838 | 2.29 | 0.1200 |  |

# Identified Patterns List: (Bookmark4)

| Visible | Ref.Code | Score | Compound Name | Displ.[°2θ] | Scale Fac. | Chem. Formula |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-012-0632 | 8 | Titanium Aluminum Carbide | -0.300 | 0.076 | Ti3 Al C2 |
| * | 04-003-0648 | 25 | Titanium Oxide | -0.300 | 0.183 | Ti O2 |
| * | 00-046-1212 | 1 | Aluminum Oxide | -0.300 | 0.055 | Al2 O3 |

# Plot of Identified Phases: (Bookmark 5)

# Document History: (Bookmark 6)

Beam attenuation factor(s) used to back-calculate ESDs:

- Modification time = "19/09/2019 09:31:41"

- Modification editor = "xrdpc2"

Insert Measurement:

- File name = "Ti3C2_20190918.xrdml"

- Modification time = "19/09/2019 09:31:41"

- Modification editor = "xrdpc2"

Default properties:

- Measurement step axis = "None"

- Internal wavelengths used from anode material: Copper (Cu)

- Original K-Alpha1 wavelength = "1.54060"

- Used K-Alpha1 wavelength = "1.54060"

- Original K-Alpha2 wavelength = "1.54443"

- Used K-Alpha2 wavelength = "1.54443"

- Original K-Beta wavelength = "1.39225"

- Used K-Beta wavelength = "1.39225"

- Fixed div. slit size = "1.00000"

- Receiving slit size = "0.10000"

- Step axis value = "0.00000"

- Offset = "0.00000"

- Sample length = "10.00000"

- Modification time = "19/09/2019 09:31:41"

- Modification editor = "xrdpc2"

Interpolate Step Size:

- Initial Scan Range = 5.00971 - 69.98310

- Initial Step Size = 0.03342

- Derived Step Size = 0.03300

- Use Derived Step Size = "Yes"

- Modification time = "19/09/2019 09:31:41"

- Modification editor = "PANalytical"

Take As Anchor Scan:

- Scan name = "Ti3C2_20190918"

- Modification time = "19/09/2019 09:40:57"

- Modification editor = "xrdpc2"

Take As Anchor Scan:

- Scan name = "Ti3C2_20190918"

- Modification time = "19/09/2019 09:41:26"

- Modification editor = "xrdpc2"

Take As Anchor Scan:

- Scan name = "Ti3C2_20190918"

- Modification time = "19/09/2019 09:41:28"

- Modification editor = "xrdpc2"

Take As Anchor Scan:

- Scan name = "Ti3C2_20190918"

- Modification time = "19/09/2019 09:57:05"

- Modification editor = "xrdpc2"

Determine Background:

- Add to net scan = "Nothing"

- User defined intensity = "-5"

- Correction method = "Automatic"

- Bending factor = "5"

- Minimum significance = "0.7"

- Minimum tip width = "0"

- Maximum tip width = "1"

- Peak base width = "2"

- Use smoothed input data = "Yes"

- Granularity = "20"

- Modification time = "22/02/2001 10:17:43"

- Modification editor = "PANalytical"

Take As Anchor Scan:

- Scan name = "Ti3C2_20190918"

- Modification time = "19/09/2019 10:43:20"

- Modification editor = "xrdpc2"

Take As Anchor Scan:

- Scan name = "Ti3C2_20190918"

- Modification time = "19/09/2019 10:56:04"

- Modification editor = "xrdpc2"

Search Peaks:

- Minimum significance = "1"

- Minimum tip width = "0.01"

- Maximum tip width = "1"

- Peak base width = "2"

- Method = "Minimum 2nd derivative"

- Modification time = "19/09/2019 10:56:17"

- Modification editor = "PANalytical"

Search & Match:

- Allow pattern shift = "Yes"

- Auto residue = "Yes"

- Data source = "Profile and peak list"

- Demote unmatched strong = "No"

- Multi phase = "Yes"

- Restriction set = "Untitled"

- Restriction = "Restriction set"

- Subset name = ""

- Match intensity = "No"

- Two theta shift = "-0.3"

- Identify = "No"

- Max. no. of accepted patterns = "5"

- Minimum score = "50"

- Min. new lines / total lines = "60"

- Search depth = "10"

- Minimum new lines = "5"

- Minimum scale factor = "0.1"

- Intensity threshold = "0"

- Use line clustering = "Yes"

- Line cluster range = "1.5"

- Search sensitivity = "1.8"

- Use adaptive smoothing = "Yes"

- Smoothing range = "1.5"

- Threshold factor = "3"

- Match Threshold = "0"

- N * Esds = "-1"

- Raw Weight = "-1"

- Peak Shape = "-1"

- Accepted Shape = "-1"

- Peak Power = "-1"

- New Peak Power = "-1"

- Intensity Power = "-1"

- N Peaks Power = "-1"

- Modification time = "19/09/2019 10:20:20"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "5.010 - 13.095"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "8"

- Chi Square = "9.69307505978574"

- Rp = "0.13722"

- Rwp = "0.19548"

- Rexp = "0.02017"

- Modification time = "19/09/2019 11:00:15"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "5.9888"

- Modification time = "19/09/2019 11:00:42"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "5.010 - 13.095"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "12"

- Chi Square = "8.01567712843994"

- Rp = "0.11158"

- Rwp = "0.16029"

- Rexp = "0.02000"

- Modification time = "19/09/2019 11:00:50"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "6.7218"

- Modification time = "19/09/2019 11:01:03"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "5.6801"

- Modification time = "19/09/2019 11:01:04"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "7.1848"

- Modification time = "19/09/2019 11:01:08"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "5.4872"

- Modification time = "19/09/2019 11:01:10"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "5.010 - 13.095"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "28"

- Chi Square = "4.86801944846253"

- Rp = "0.06279"

- Rwp = "0.09396"

- Rexp = "0.01930"

- Modification time = "19/09/2019 11:01:21"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "15.675 - 24.453"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "8"

- Chi Square = "0.981293793624053"

- Rp = "0.01796"

- Rwp = "0.02267"

- Rexp = "0.02310"

- Modification time = "19/09/2019 11:01:38"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "21.450 - 31.779"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "12"

- Chi Square = "8.52309741586522"

- Rp = "0.10413"

- Rwp = "0.16184"

- Rexp = "0.01899"

- Modification time = "19/09/2019 11:01:46"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "29.958 - 40.287"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "28"

- Chi Square = "4.30802011361371"

- Rp = "0.04426"

- Rwp = "0.06638"

- Rexp = "0.01541"

- Modification time = "19/09/2019 11:02:04"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "39.726 - 50.055"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "20"

- Chi Square = "3.81486995296546"

- Rp = "0.04614"

- Rwp = "0.06376"

- Rexp = "0.01671"

- Modification time = "19/09/2019 11:02:18"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "40.9882"

- Modification time = "19/09/2019 11:02:49"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "40.095 - 42.768"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "12"

- Chi Square = "4.45909326307541"

- Rp = "0.04673"

- Rwp = "0.05858"

- Rexp = "0.01314"

- Modification time = "19/09/2019 11:03:06"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "51.084 - 58.938"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "20"

- Chi Square = "8.6801412602609"

- Rp = "0.09785"

- Rwp = "0.14253"

- Rexp = "0.01642"

- Modification time = "19/09/2019 11:04:20"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "56.985 - 58.635"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "4"

- Chi Square = "0.983453614182153"

- Rp = "0.01394"

- Rwp = "0.01763"

- Rexp = "0.01793"

- Modification time = "19/09/2019 11:04:52"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "58.344 - 64.647"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "16"

- Chi Square = "4.36853089507383"

- Rp = "0.04990"

- Rwp = "0.07181"

- Rexp = "0.01644"

- Modification time = "19/09/2019 11:05:16"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "60.8959"

- Modification time = "19/09/2019 11:06:10"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "59.493 - 61.737"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "16"

- Chi Square = "4.54068336772865"

- Rp = "0.04843"

- Rwp = "0.06301"

- Rexp = "0.01388"

- Modification time = "19/09/2019 11:06:18"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "61.3706"

- Modification time = "19/09/2019 11:07:00"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "59.493 - 61.737"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "20"

- Chi Square = "3.45877817329938"

- Rp = "0.03681"

- Rwp = "0.04615"

- Rexp = "0.01334"

- Modification time = "19/09/2019 11:07:06"

- Modification editor = "xrdpc2"

Insert Peak:

- Peak position Gonio = "63.4214"

- Modification time = "19/09/2019 11:09:08"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "62.040 - 64.647"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "8"

- Chi Square = "2.84216972521445"

- Rp = "0.03460"

- Rwp = "0.04751"

- Rexp = "0.01671"

- Modification time = "19/09/2019 11:09:15"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "64.938 - 67.545"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "8"

- Chi Square = "1.40116270904577"

- Rp = "0.01828"

- Rwp = "0.02548"

- Rexp = "0.01818"

- Modification time = "19/09/2019 11:09:42"

- Modification editor = "xrdpc2"

Profile/Rietveld fitting:

- Angular range Gonio = "67.347 - 69.954"

- Step No. 1

- Title = "Flat Background"

- Switch off after usage = "False"

- Step No. 2

- Title = "More background"

- Switch off after usage = "False"

- No. additional parameters = "2"

- Use 1/X background too = "True"

- Step No. 3

- Title = "Peak Position"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 4

- Title = "Peak Area"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 5

- Title = "Peak FWHM"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- Step No. 6

- Title = "Peak Shape"

- Switch off after usage = "False"

- Minimum Irelative % = "-1"

- No. of refined parameters = "8"

- Chi Square = "4.48945977694756"

- Rp = "0.05895"

- Rwp = "0.07377"

- Rexp = "0.01643"

- Modification time = "19/09/2019 11:09:51"

- Modification editor = "xrdpc2"

Take As Anchor Scan:

- Scan name = "Ti3C2_20190918"

- Modification time = "19/09/2019 11:33:21"

- Modification editor = "xrdpc2"