## Slide 1: QUE 99177 Ch6_004
Extracted data from maps

## Slide 2: QUE 99177 Ch6_004- Lpx extraction
MgO wt% map
Filters on map:
MgO wt%>30<40
Total >98.5<102
Pixel width 10

## Slide 3: QUE 99177 Ch6_004- Cpx extraction
CaO wt% map
Filters on map:
CaO wt% >13<20
Al2O3 wt% >0<5
Total >98.5<102
Pixel width 10
Al2O3 wt% filter to try an avoid sampling from the surrounding plag grains

## Slide 4: QUE 99177 Ch6_004- Plag extraction
Al2O3 wt% map
Filters on map:
Na2O wt% >3<5.7
SiO2>52<58
Al2O3 wt% >26<31
Total >98.5<102
Pixel width 10
Si filter to try an avoid sampling from the surrounding Si-glass. Na and Al filter used to define the plag

## Slide 5: QUE 99177 Ch6_004- Si-glass extraction (Si on Wol)
SiO2 wt% map
Filters on map:
SiO2>70<90
Al2O3 wt% >12<14.5
Total >98.5<102
Pixel width 10
Al filter to try an avoid sampling from the surrounding plag. Si used to define the Si-rich glass region

## Slide 6: QUE 99177 Ch6_004- Si-glass extraction (Si on Qtz)
SiO2 wt% map
Filters on map:
SiO2>70<90
Al2O3 wt% >12<14.5
Total >98.5<102
Pixel width 10
Al filter to try an avoid sampling from the surrounding plag. Si used to define the Si-rich glass region