## Slide 1: MET 00426 Ch3_001
Data extracted from maps

## Slide 2: MET 00426 Ch3_001 Silica grain extraction
SiO2 wt% map
Filters:
SiO2 wt% >95<102
FeO wt% >0<1
Total >98.5<102
Pixel width 10
Fe filter to avoid interaction with Fe veining. Si filter to define silica grains.

## Slide 3: MET 00426 Ch3_001 Cpx Rim extraction
CaO wt% map
Filters:
CaO wt% >10<20.5
Total >98.5<102
Pixel width 10
CaO filter to define Cpx grains

## Slide 4: MET 00426 Ch3_001 Glass Rim extraction
Al2O3 wt% map
Filters:
SiO2 wt% >55<85
FeO wt%>0<2
Total >98.5<102
Pixel width 10
SiO2 filter to define glass region and FeO filter to lmit interaction from Fe grains and Fe veining

## Slide 5: MET 00426 Ch3_001 Lpx Core extraction
MgO wt% map
Filters:
MgO wt% >30<40.5
FeO wt%>0<3
Total >98.5<102
Pixel width 10
MgO filter to define Lpx grains and FeO filter to limit interaction from surrounding Fe grains and Fe veining

## Slide 6: MET 00426 Ch3_001 Cpx Core extraction
CaO wt% map
Filters:
SiO2 wt% >30<60
CaO wt% >8<14
FeO wt%>0<3
Total >98.5<102
Pixel width 10
CaO filter to define Cpx grains and FeO filter to limit interaction from surrounding Fe veining. SiO2 filter to limit interaction form surrounding Si-rich glass

## Slide 7: MET 00426 Ch3_001 Glass Core Extraction
Al2O3 wt% map
Filters:
SiO2 wt% >60<75
Al2O3 wt% >10<20
FeO wt%>0<2
Total >98.5<102
Pixel width 10
SiO2 and Al2O3 filter to define glass. FeO filter to limit interaction from surrounding metal grains and Fe veining

## Slide 8: MET 00426 Ch3_001 Intermediate pyx core extraction
CaO wt% map
Filters:
SiO2 wt% >30<60
CaO wt% >8<14
FeO wt%>0<3
Total >98.5<102
Pixel width 10
CaO filter to define Cpx grains and FeO filter to limit interaction from surrounding Fe veining. SiO2 filter to limit interaction form surrounding Si-rich glass